| PN (PN): |  | SN: |  |  |  | Nº da OS (WO): |  |  | TLN: |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 6879879 |  | 27553 |  |  |  | 035590 |  |  | 02118 |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  | ARTIGO/PARTE (Article/Part): |  |  |  | QUANT: |  |  |
| M250-C20J / Avulso |  |  | Exhaust Collector Support |  |  |  | 01 EA |  |  |
| TSN: N/A |  |  | CSN: N/A |  | TSO: N/A |  | CSO: N/A |  |  |
| ITEM (Item) | DESCRIÇÃO DO SERVIÇO A EXECUTAR (Description of the work to be executed) |  |  |  |  | EXECUÇÃO (Execution) |  |  | *SETOR/FORNECEDOR (Sector/Supplier) |
|  | Service requested: Repair Dim RG, Dia BA, Dia M and surface P per OHM 10W3 and PRPL 2-D001. |  |  |  |  |  |  |  |  |
| 1 | Realizar inspeção dimensional, conforme OHM 10W3. Perform dimensional inspection, according to OHM 10W3. |  |  |  |  |  |  |  | Inspeção Dimensional Dimensional Inspection |
| 2 | Analisar laudo dimensional, conforme OHM 10W3, e realizar visual do artigo. Analyze dimensional report, according to OHM 10W3, and perform visual of the article. |  |  |  |  |  |  |  | Engenharia Engineering |
| 3 | Usinar “Diâmetro BA”, “Diâmetro M” e “Superfície P” para remover todo o níquel existente, conforme PRPL 2-D001. Machine “Diameter BA”, “Diameter M” and “Surface P” to remove all existing nickel, according to PRPL 2-D001. |  |  |  |  |  |  |  | Usinagem Machining |
| 4 | Preparar Retaining Ring Groove (“DIM RG”) para soldagem, conforme PRPL 2-D001. Prepare Retaining Ring Groove (“DIM RG”) for welding, according to PRPL 2-D001. |  |  |  |  |  |  |  | Usinagem Machining |
| 5 | Realizar limpeza da peça, conforme IAS-IP-0006; Item 3.34; Rev. 03. Clean the part, according to IAS-IP-0006; Item 3.34; Rev. 03. |  |  |  |  |  |  |  | Limpeza Química Chemical Cleaning |
| 6 | Realizar NDT local, conforme OHM 10W3, nos locais trabalhados de acordo com etapas anteriores. (Perform local NDT, according to OHM 10W3, in the areas worked according to previous steps.) Ensaio (Test): FPI Tipo (Type): 1 Método (Method): A Sensibilidade (Sensitivity): 2 Foram encontradas indicações? (Were Indications found?) ( ) SIM: REGISTRAR IAS-RG-0332 (YES: REGISTER IAS-RG-0332) ( ) NÃO: PROSSEGUIR PARA PRÓXIMA ETAPA (NO: PROCEED TO NEXT STEP) |  |  |  |  |  |  |  | NDT |
| 7 | Realizar inspeção pós NDT, conforme OHM 10W3. Referir-se aos resultados registrados no formulário IAS-RG-0332 (se feito na etapa anterior) e preencher o mesmo com as devidas observações. Avaliar os limites de aceitação, conforme OHM 10W3. Perform post-NDT inspection, according to OHM 10W3. Refer to the results recorded in the IAS-RG-0332 form (if done in the previous step) and fill it out with the appropriate observations. Assess the acceptance limits, according to OHM 10W3. ( ) APROVADO (APPROVED) ( ) REJEITADO (REJECTED) |  |  |  |  |  |  |  | Inspeção Inspection |
| 8 | Realizar limpeza pós NDT, conforme IAS-IP-0006; Item 3.34; Rev. 03. Perform post-NDT cleaning, according to IAS-IP-0006; Item 3.34; Rev. 03. |  |  |  |  |  |  |  | Limpeza química Chemical Cleaning |
| 9 | Realizar inspeção dimensional, conforme OHM 10W3. Perform dimensional inspection, according to OHM 10W3. |  |  |  |  |  |  |  | Inspeção Dimensional Dimensional Inspection |
| 10 | Analisar laudo dimensional, conforme OHM 10W3, e realizar visual do artigo. Analyze dimensional report, according to OHM 10W3, and perform visual of the article. |  |  |  |  |  |  |  | Engenharia Engineering |
| 11 | Desenvolver e fabricar ferramenta visando diminuição de ovalização de dimensões próximas ao Retaining Ring Groove quando é feita sua soldagem. Develop and manufacture a tool aimed at reducing ovalization of dimensions close to the Retaining Ring Groove when welding. |  |  |  |  |  |  |  | Reparos Repairs |
| 12 | Encaminhar ferramenta e peça para a Engenharia para que sejam analisadas e seja aberta nova sub O.S. referente a continuação dos reparos e processos Forward the tool and part to Engineering for analysis and a new sub-O.S. to be opened regarding the continuation of repairs and processes. |  |  |  |  |  |  |  | Controller |
| OBSERVAÇÕES (Observation): |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  | DATA (Date): |  |
|  |  |  |  | Pedro Costa |  |  |  | 08/08/2024 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)