| PN (PN): |  | SN: |  |  |  | Nº da OS (WO): |  |  |  | TLN: |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 23059598 |  | FU39945 |  |  |  | 035867 |  |  |  | 02118 |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  | ARTIGO/PARTE (Article/Part): |  |  |  |  | QUANT: |  |  |
| M250-C20J / CAE-270840 |  |  | Scroll assy |  |  |  |  | 01 EA |  |  |
| TSN: N/A |  |  | CSN: N/A |  | TSO: N/A |  |  | CSO: N/A |  |  |
| ITEM (Item) | DESCRIÇÃO DO SERVIÇO A EXECUTAR (Description of the work to be executed) |  |  |  |  |  | EXECUÇÃO (Execution) |  |  | *SETOR/FORNECEDOR (Sector/Supplier) |
|  | Service requested by the customer: Glass bead, replace air tube insert and chase theads per OHM 10W3. |  |  |  |  |  |  |  |  |  |
| 1 | Remover air insert tubes e realizar limpeza das roscas, dos prisioneiros do scroll e repassar de onde foram dos air inserts tubes. Remove air insert tubes and tap thread holes and studs of the part. |  |  |  |  |  |  |  |  | Reparos manuais |
| 2 | Isolar locais onde não será jateado e realizar jateamento com casca de noz e pressão de até 40 PSI nos locais com corrosão. Mask all areas other the places that will be blasted and blast with Walnut Shell, don’t exceed 40 PSI on corroded areas. |  |  |  |  |  |  |  |  | Limpeza química |
| 3 | Realizar limpeza conforme IAS-IP-0006 Item 3.34 Rev.03. Perform clean per IAS-IP-0006 Item 3.34 Rev.03. |  |  |  |  |  |  |  |  | Limpeza química |
| 4 | Preparar para instalação dos Air tube inserts, aplicar uma camada fina e uniforme de selante nas roscas internas (EPOXYLITE814, PLASTISEAL F OU EQUIVALENTE. (Ref. PRPL2-B0001 / 2.A.3)). Apply a thin uniform coat of high temperature joint sealing compound to the internal threads of the bore prior to insert installation. (EPOXYLITE814, PLASTISEAL F OR EQUIVALENT. (Ref. PRPL2-B0001 / 2.A.3)) |  |  |  |  |  |  |  |  | M250 & RR300 |
| 5 | Instalar Air tube insert novos e utilizar a ferramenta 6872272 para aplicar torque de 40--50 lb ft (54-67 N.m). Install the new inserts. Torque to 40--50 lb ft (54-67 N.m) using wrench (6872272). Torque value: _______________. NCC: _________________. Valid until: _____________. |  |  |  |  |  |  |  |  | M250 & RR300 |
| 6 | Frenar o Air insert tube no scroll locking retention slot. Depress insert flange into slot for locking retention. |  |  |  |  |  |  |  |  | M250 & RR300 |
| 7 | Inspeção final. Final inspection. |  |  |  |  |  |  |  |  | Inspeção |
| OBSERVAÇÕES (Observation): |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  |  | DATA (Date): |  |
|  |  |  |  | Patrick Dimas |  |  |  |  | 30/07/2024 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)