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	CODIGO | CODE
	SOLICITAÇÃO DE SERVIÇOS COMPLEMENTARES
	PÁGINA
	1/1

	IAS-RG-0103
	SUPPLEMENTARY REQUEST
	PAGE
	



	PN (PN):
	SN:
	Nº da OS (WO):
	TLN:

	23076529
	GK559132
	037372
	02127

	Nº DO ARTIGO PRINCIPAL (Main Article):
	ARTIGO/PARTE (Article/Part):
	QUANT:

	M2450-C47B / CAT-45949
	Turbine Spline Adapter
	01 EA

	TSN: N/A
	CSN: N/A
	TSO: N/A
	CSO: N/A

	ITEM
(Item)
	DESCRIÇÃO DO SERVIÇO A EXECUTAR
 (Description of the work to be executed)
	EXECUÇÃO
(Execution)
	*SETOR/FORNECEDOR
(Sector/Supplier)

	
	Service requested by the customer:
Restore Silver Plating per OHM CSP22001.

	1
	Restaure banho de prata nas estrias externas com uma espessura de 0,0001-0,0003 pol. (0,003-0,008 mm) (Ref. AMS 2410 ou AMS 2412). 

Restore the silver plate to the external splines to a thickness of 0.0001-0.0003 in. (0.003-0.008 mm) (Ref. AMS 2410 or AMS 2412).
	
	Galvanoplastia

	2
	Dentro de quatro horas após o banho, faça o alívio da fragilização por hidrogênio aquecido a 350-550°F (177-288°C) durante duas horas (Ref. AMS 2410 ou AMS 2412).

Within four hours after you plate, do the hydrogen enbrittlement relief heated to 350-550°F (177-288°C) for two hours (Ref. AMS 2410 or AMS 2412).
	
	Galvanoplastia

	3
	Inspeção final.

Final inspection.
	
	Inspeção

	
	
	
	

	OBSERVAÇÕES
(Observation):
	ASSINATURA DO SOLICITANTE 
(Signature):
	DATA 
(Date):

	
	Patrick Dimas
	27/08/2024


· Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.
(In case of external service, the supplier must be indicated by the purchasing department)
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