| PN (PN): |  | SN: |  |  |  | Nº da OS (WO): |  |  |  | TLN: |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 23076529 |  | GK559132 |  |  |  | 037372 |  |  |  | 02127 |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  | ARTIGO/PARTE (Article/Part): |  |  |  |  | QUANT: |  |  |
| M2450-C47B / CAT-45949 |  |  | Turbine Spline Adapter |  |  |  |  | 01 EA |  |  |
| TSN: N/A |  |  | CSN: N/A |  | TSO: N/A |  |  | CSO: N/A |  |  |
| ITEM (Item) | DESCRIÇÃO DO SERVIÇO A EXECUTAR (Description of the work to be executed) |  |  |  |  |  | EXECUÇÃO (Execution) |  |  | *SETOR/FORNECEDOR (Sector/Supplier) |
|  | Service requested by the customer: Restore Silver Plating per OHM CSP22001. |  |  |  |  |  |  |  |  |  |
| 1 | Restaure banho de prata nas estrias externas com uma espessura de 0,0001-0,0003 pol. (0,003-0,008 mm) (Ref. AMS 2410 ou AMS 2412). Restore the silver plate to the external splines to a thickness of 0.0001-0.0003 in. (0.003-0.008 mm) (Ref. AMS 2410 or AMS 2412). |  |  |  |  |  |  |  |  | Galvanoplastia |
| 2 | Dentro de quatro horas após o banho, faça o alívio da fragilização por hidrogênio aquecido a 350-550°F (177-288°C) durante duas horas (Ref. AMS 2410 ou AMS 2412). Within four hours after you plate, do the hydrogen enbrittlement relief heated to 350-550°F (177-288°C) for two hours (Ref. AMS 2410 or AMS 2412). |  |  |  |  |  |  |  |  | Galvanoplastia |
| 3 | Inspeção final. Final inspection. |  |  |  |  |  |  |  |  | Inspeção |
| OBSERVAÇÕES (Observation): |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  |  | DATA (Date): |  |
|  |  |  |  | Patrick Dimas |  |  |  |  | 27/08/2024 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)