	[image: Logotipo

Descrição gerada automaticamente]
	REGISTRO
	REVISÃO
	02

	
	RECORD
	REVISION
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	SOLICITAÇÃO DE SERVIÇOS COMPLEMENTARES
	PÁGINA
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	PN (PN):
	SN:
	Nº da OS (WO):
	TLN:

	RR30000246
	GK25189
	037808
	TLN02027

	Nº DO ARTIGO PRINCIPAL (Main Article):
	ARTIGO/PARTE (Article/Part):
	QUANT:

	RRE-200093
	ADAPTADOR ESTRIADO
	01

	TSN:                                         -----------
	CSN:                  -------
	TSO:                ----------
	CSO:                   -----------

	

	ITEM
(Item)
	DESCRIÇÃO DO SERVIÇO A EXECUTAR
 (Description of the work to be executed)
	EXECUÇÃO
(Execution)
	*SETOR/FORNECEDOR
(Sector/Supplier)

	Service requested:
Restore Silver

	01
	Restaure revestimento de prata nas estrias externas com uma espessura de 0,0001-0,0003 pol.
(0,003-0,008 mm) (Ref. AMS 2410 ou AMS 2412). 

Restore the silver plate to the external splines to a thickness of 0.0001-0.0003 in. (0.003-0.008 mm) (Ref. AMS 2410 or AMS 2412).
	
	GALVANOPLASTIA

	02
	Dentro de quatro horas após o banho, faça o alívio da fragilização por hidrogênio aquecido a 350-550°F
(177-288°C) durante duas horas (Ref. AMS 2410 ou AMS 2412).

Within four hours after you plate, do the hydrogen enbrittlement relief heated to 350-550°F
(177-288°C) for two hours (Ref. AMS 2410 or AMS 2412).
	
	GALVANOPLASTIA

	03
	Inspeção Final.

Final inspection.
	
	INSPEÇÃO

	
	
	
	

	OBSERVAÇÕES
(Observation):
	ASSINATURA DO SOLICITANTE 
(Signature):
	DATA	
DATE

09/09/2024

	Figure 801 attached
	Luan Gomes
	


· Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.
(In case of external service, the supplier must be indicated by the purchasing department)
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