| PN (PN): |  | SN: |  |  |  | Nº da OS (WO): |  |  |  |  | TLN: |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| RR30000246 |  | GK25189 |  |  |  | 037808 |  |  |  |  | TLN02027 |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  | ARTIGO/PARTE (Article/Part): |  |  |  |  |  | QUANT: |  |  |
| RRE-200093 |  |  | ADAPTADOR ESTRIADO |  |  |  |  |  | 01 |  |  |
| TSN: ----------- |  |  | CSN: ------- |  | TSO: ---------- |  |  |  | CSO: ----------- |  |  |
| ITEM (Item) | DESCRIÇÃO DO SERVIÇO A EXECUTAR (Description of the work to be executed) |  |  |  |  |  | EXECUÇÃO (Execution) | *SETOR/FORNECEDOR (Sector/Supplier) |  |  |  |
| Service requested: Restore Silver |  |  |  |  |  |  |  |  |  |  |  |
| 01 | Restaure revestimento de prata nas estrias externas com uma espessura de 0,0001-0,0003 pol. (0,003-0,008 mm) (Ref. AMS 2410 ou AMS 2412). Restore the silver plate to the external splines to a thickness of 0.0001-0.0003 in. (0.003-0.008 mm) (Ref. AMS 2410 or AMS 2412). |  |  |  |  |  |  | GALVANOPLASTIA |  |  |  |
| 02 | Dentro de quatro horas após o banho, faça o alívio da fragilização por hidrogênio aquecido a 350-550°F (177-288°C) durante duas horas (Ref. AMS 2410 ou AMS 2412). Within four hours after you plate, do the hydrogen enbrittlement relief heated to 350-550°F (177-288°C) for two hours (Ref. AMS 2410 or AMS 2412). |  |  |  |  |  |  | GALVANOPLASTIA |  |  |  |
| 03 | Inspeção Final. Final inspection. |  |  |  |  |  |  | INSPEÇÃO |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  |  |  | DATA DATE 09/09/2024 |  |
| Figure 801 attached |  |  |  | Luan Gomes |  |  |  |  |  |  |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)