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	RECORD
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	CODIGO | CODE
	SOLICITAÇÃO DE SERVIÇOS COMPLEMENTARES
	PÁGINA
	1/1

	IAS-RG-0103
	SUPPLEMENTARY REQUEST
	PAGE
	



	PN 
	SN:
	Nº da OS      ¨IAS¨
	TLN:02188

	23072258
	                       KK35016
	
	

	Nº DO ARTIGO PRINCIPAL (Main Article):
	ARTIGO/PARTE (Article/Part):
	QUANT:

	                    COMPRESSOR AE-109020
	                      WHEEL 14º ST
	1

	
	
	
	

	ITEM
(Item)
	DESCRIÇÃO DO SERVIÇO A EXECUTAR
 (Description of the work to be executed)
	EXECUÇÃO
(Execution)
	*SETOR/FORNECEDOR
(Sector/Supplier)

	1
	REMOVER AS 20 PALHETAS REFUGOS, ASSINALADAS DE VERMELHO E ENSACAR SEPARADAS DAS DEMAIS BOAS.

REMOVE THE 20 SCRAP STRAWS, MARKED IN RED AND BAG SEPARATELY FROM THE OTHER GOOD ONES
	
	REPAROS

	2
	REMOVER O CONTRA PESO E SUAVISAR OS FUROS DO LIP.

REMOVE THE COUNTERWEIGHT AND SMOOTH THE LIP HOLES
	
	REPAROS

	3
	REMOVER AS DEMAIS PALHETAS, CUIDANDO PARA NÃO DANIFICA-LAS, POIS SERÃO REUSADAS.

REMOVE THE OTHER BLADES, TAKING CARE NOT TO DAMAGE THEM, AS THEY WILL BE REUSED
	
	REPAROS

	4
	TIRAR OS PEDAÇOS DE PINOS DA RODA E DAS PALHETAS BOAS E AS REBARBAS ADJACENTES.

REMOVE THE PIECES OF PINS FROM THE WHEEL AND THE GOOD VANES AND THE ADJACENT BURRS
	
	REPAROS

	5
	EXECUTAR LIMPEZA DA RODA E DAS PALHETAS BOAS, CONFORME A IP-0006, 3.8

CLEAN THE WHEEL AND GOOD VANES ACCORDING TO IP-0006, 3.
	
	LIMPEZA

	6
	EXECUTAR FPI: ASTM E 1417, METHOD-D, LEVEL-4
APRESENTOU INDICAÇÕES? (  )SIM           (  )NÃO

RUN FPI: ASTM E 1417, METHOD-D, LEVEL-4 DID YOU PRESENT INDICATIONS? ( )YES ( )N
	
	NDT

	7
	LIMPAR CONFORME A IP-0006, 3.10

CLEAR AS PER IP-0006, 3.1
	
	LIMPEZA

	8
	ISOLAR E APLICAR BANHO DE PRATA NA ROSCA INTERNA, AMS 2410.

ISOLATE AND APPLY SILVER PLATING ON THE INTERNAL THREAD, AMS 2410
	
	GALVANO

	9
	CRIAR O.S. PARA AS PALHETAS BOAS APÓS INSPECIONA-LAS.

CREATE O.S. FOR THE GOOD VANES AFTER INSPECTING THEM
	
	INSPEÇÃO

	10
	MONTAR AS PALHETAS, FRENA-LAS COM PINOS P/N=6731108  E EXECUTAR STAK.

ASSEMBLE THE BLADES, BRAKE THEM WITH PINS P/N=6731108 AND PERFORM STAK
	
	REPAROS

	11
	INSPEÇÃO FINAL.
(  )APROVADO        (  )REPROVADO

FINAL INSPECTION. ( )APPROVED ( )FAILE
	
	INSPEÇÃO

	OBSERVAÇÕES
(Observation):
	ASSINATURA DO SOLICITANTE 
(Signature):   VILSON BARBOSA
	DATA 
(Date):   15/10/2024

	[bookmark: Texto2]     
	VILSON BARBOSA
	15/10/2024


· Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.
(In case of external service, the supplier must be indicated by the purchasing department)
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