| PN (PN): |  | SN: |  |  |  | Nº da OS (WO): |  |  |  | TLN: |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| RR30000416 |  | JE62996 |  |  |  | 038823 |  |  |  | 02027 |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  | ARTIGO/PARTE (Article/Part): |  |  |  |  | QUANT: |  |  |
| RR300 / RRE-200226 |  |  | Scroll Assy |  |  |  |  | 01 EA |  |  |
| TSN: N/A |  |  | CSN: N/A |  | TSO: N/A |  |  | CSO: N/A |  |  |
| ITEM (Item) | DESCRIÇÃO DO SERVIÇO A EXECUTAR (Description of the work to be executed) |  |  |  |  |  | EXECUÇÃO (Execution) |  |  | *SETOR/FORNECEDOR (Sector/Supplier) |
|  | Service requested by the customer: Treat corrosion per HMM CSP22005. |  |  |  |  |  |  |  |  |  |
|  | Remover nickel conforme AMS 2404. Remove the nickel per AMS 2404. |  |  |  |  |  |  |  |  | Galvanoplastia |
|  | Realizar a remoção do bleed port fitting danificado conforme ERPM TASK 72-30-30-300-801. Remove the damaged bleed port fitting as per ERPM TASK 72-30-30-300-801. |  |  |  |  |  |  |  |  | Limpeza química |
|  | Realizar a fabricação do bleed port fitting conforme ERPM TASK 72-30-30-300-801. Figura 902 Manufacture the bleed port fitting according to ERPM TASK 72-30-30-300-801. Figure 902 |  |  |  |  |  |  |  |  |  |
|  | Soldar o novo fitting conforme ERPM TASK 72-30-30-300-801 Weld the new fitting according to ERPM TASK 72-30-30-300-801 |  |  |  |  |  |  |  |  | Reparos manuais |
|  | Fixar o scroll em uma ferramenta fabricada na IAS para realizar Alivio de tensão Fix the scroll to a tool manufactured at IAS to perform stress relief |  |  |  |  |  |  |  |  | Reparos manuais |
|  | Realizar alívio de tensão conforme tabela 901 do ERPM TASK 72-30-30-300-801. Perform voltage relief according to table 901 of ERPM TASK 72-30-30-300-801 |  |  |  |  |  |  |  |  |  |
|  | Realizar limpeza conforme IAS-IP-0006 Item 3.35 Rev.03. Perform cleaning per IAS-IP-0006 Item 3.35 Rev.03. |  |  |  |  |  |  |  |  | Limpeza química |
|  | Realizar NDT conforme indicado no (Perform NDT conform indicated in the.) Heavy Maintenance Manual CSP22005. Ensaio (Test): FPI Tipo (Type): 1 Método (Method): A Sensibilidade (Sensitivity): 3 Foram encontradas indicações? (Were Indications found?) ( ) SIM – REGISTRAR IAS-RG-0332. (YES – REGISTRAR IAS-RG-0332.) ( ) NÃO – PROCESSEGUIR PARA ETAPA DE LIMPEZA PÓS NDT (NO – PROCEED TO THE AFTER NDT CLEANING STEP.) |  |  |  |  |  |  |  |  | NDT |
| 8 | Realizar inspeção pós NDT conforme. (Perform inspection after NDT iaw) Manual. Refira-se aos resultados registrados no RG-0332 (se foi feito na etapa anterior) e preencher o mesmo com devidas observações. (Refer to the results registered in the RG-0332 (if it was done in the step before) and fill it in with due observations). Avaliar os limites de aceitação conforme OMM. (Evaluate the acceptance limits conform OMM.) ( ) APROVADO – (APPROVED) ( ) REJEITADO – (REJECTED) |  |  |  |  |  |  |  |  | Inspeção |
| 9 | Realizar limpeza pós NDT conforme IAS-IP-0006 item 3.34 Rev.03. Perform Cleaning after NDT IAW IAS-IP-0006 item 3.34 Rev.03. |  |  |  |  |  |  |  |  | Limpeza química |
| 10 | Aplicar nickel conforme AMS 2404, não aplicar nickel nas roscas e nos studs. Apply nickel per AMS 2404, don’t apply nickel on studs and threads. |  |  |  |  |  |  |  |  | Galvanoplastia |
| 11 | Inspeção final. Final inspection. |  |  |  |  |  |  |  |  | Inspeção |
| OBSERVAÇÕES (Observation): |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  |  | DATA (Date): |  |
|  |  |  |  | Antonio Claudio |  |  |  |  | 31/10/24 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)