| PN |  | SN: |  |  | Nº da OS ¨IAS¨ |  |  |  |  | TLN:02188 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 6873732 |  | GGK582 |  |  |  |  |  |  |  |  |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  | ARTIGO/PARTE (Article/Part): |  |  |  |  | QUANT: |  |  |
| AE-109696 - AGO29500 |  |  | BEARING SEPARATOR |  |  |  |  | 1 |  |  |
| ITEM (Item) | DESCRIÇÃO DO SERVIÇO A EXECUTAR (Description of the work to be executed) |  |  |  |  | EXECUÇÃO (Execution) | *SETOR/FORNECEDOR (Sector/Supplier) |  |  |  |
| 1 | REMOVER O BANHO DE PRATA COM GLASS BEAD, IP-0006, 3.26 NOTA: ESTE MATERIAL É COBRE. REMOVE SILVER PLATED WITH GLASS BEAD, IP-0006, 3.26 NOTE: THIS MATERIAL IS COPPER. |  |  |  |  |  | LIMPEZA |  |  |  |
| 2 | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  | LIMPEZA |  |  |  |
| 3 | EXECUTAR FPI: ASTM E 1417, METHOD-D, LEVEL 4. APRESENTOU INDICAÇÃO? ( )SIM ( )NÃO EXECUTAR FPI: ASTM E 1417, METHOD-D, LEVEL 4. APRESENTOU INDICAÇÃO? ( )SIM ( )NÃO |  |  |  |  |  | NDT |  |  |  |
| 4 | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  | LIMPEZA |  |  |  |
| 5 | APLICAR BANHO DE PRATA COM A ESPESSURA O DOBRO QUE COSTUMAM DAR EM PARAFUSOS. IT-0279. NOTA: ESTE MATERIAL É COBRE. APPLY SILVER PLATING WITH THE THICKNESS TWICE AS THICK AS THEY USUALLY GIVE IN SCREWS. IT-0279. NOTE: THIS MATERIAL IS COPPER. |  |  |  |  |  | GALVANO |  |  |  |
| 6 | INSPEÇÃO FINAL. ( )APROVADO ( )REPROVADO FINAL INSPECTION. ( )APPROVED ( )FAILED |  |  |  |  |  | INSPEÇÃO FINAL |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  | ASSINATURA DO SOLICITANTE (Signature): VILSON BARBOSA |  |  |  |  | DATA (Date): 18/11/2024 |  |
|  |  |  |  | VILSON BARBOSA |  |  |  |  | 18/11/2024 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)