| PN |  | SN: |  |  | Nº da OS ¨IAS¨ |  |  |  |  | TLN:02188 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 6873732 |  | GGK582 |  |  |  |  |  |  |  |  |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  | ARTIGO/PARTE (Article/Part): |  |  |  |  | QUANT: |  |  |
| AE-109696 - AGO-29500 |  |  | BEARING INNER RACE - |  |  |  |  | 1 |  |  |
| ITEM (Item) | DESCRIÇÃO DO SERVIÇO A EXECUTAR (Description of the work to be executed) |  |  |  |  | EXECUÇÃO (Execution) | *SETOR/FORNECEDOR (Sector/Supplier) |  |  |  |
| 1 | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  | LIMPEZA |  |  |  |
| 2 | EXECUTAR MPI: ASTM E 1444. APRESENTOU INDICAÇÃO? ( )SIM ( )NÃO RUN MPI: ASTM E 1444. DID YOU PRESENT AN INDICATION? ( )YES ( )NO |  |  |  |  |  | NDT |  |  |  |
| 3 | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  | LIMPEZA |  |  |  |
| 4 | ISOLAR E APLICAR 0.0004¨ESPESSURA DE BANHO DE COBRE NO DIÂMETRO INTERNO. NOTA: CUIDADO COM A ISOLAÇÃO, POIS JÁ HOUVE INFILTRAÇÃO E DANIFICAÇÃO EM ALGUNS CASOS. ISOLATE AND APPLY 0.0004 ̈COPPER BATH THICKNESS ON THE INNER DIAMETER. NOTE: BE CAREFUL WITH THE INSULATION, AS THERE HAS ALREADY BEEN INFILTRATION AND DAMAGE IN SOME CASES. |  |  |  |  |  | GALVANO |  |  |  |
| 5 | INSPEÇÃO FINAL. ( )APROVADO ( )REPROVADO FINAL INSPECTION. ( )APPROVED ( )FAILED |  |  |  |  |  | INSPEÇÃO |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  | ASSINATURA DO SOLICITANTE (Signature): VILSON BARBOSA |  |  |  |  | DATA (Date): 18/11/2024 |  |
|  |  |  |  | VILSON BARBOSA |  |  |  |  | 18/11/2024 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)