| PN |  | SN: |  |  | Nº da OS |  |  |  |  | TLN:02188 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 6894068 |  | 10345 |  |  |  |  |  |  |  | TASK 72-47-00-300-801 |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  | ARTIGO/PARTE (Article/Part): |  |  |  |  | QUANT: |  |  |
| 750585 |  |  |  |  |  |  |  | 1 |  |  |
| ITEM (Item) | DESCRIÇÃO DO SERVIÇO A EXECUTAR (Description of the work to be executed) |  |  |  |  | EXECUÇÃO (Execution) | *SETOR/FORNECEDOR (Sector/Supplier) |  |  |  |
| 1 | EXECUTAR TRATAMENTO TÉRMICO EM 1010°C, POR 30 MINUTOS. PERFORM HEAT TREATMENT AT 1010°C FOR 30 MINUTES. |  |  |  |  |  | REPAROS |  |  |  |
| 2 | PREPARAR E SOLDAR TRINCAS INTERNAS MARCADAS NA AREA DE JUNÇÃO DA TRANSITION SECTION. AMS-5798 SOLDAR TRINCA INTERNA MARCADA NA AREA DE ESCAPE. AMS-5798. SUAVISAR TODAS AS SOLDAS. TASK 72-47-00-300-801 PREPARE AND WELD INTERNAL CRACKS MARKED IN THE JOINT AREA OF THE TRANSITION SECTION. AMS-5798 WELD INTERNAL CRACK MARKED IN THE EXHAUST AREA. AMS-5798. SMOOTH ALL WELDINGS. TASK 72-47-00-300-801 |  |  |  |  |  | SOLDAGEM |  |  |  |
| 3 | EXECUTAR TRATAMENTO TÉRMICO EM 1010°C, POR 30 MINUTOS. PERFORM HEAT TREATMENT AT 1010°C FOR 30 MINUTES. |  |  |  |  |  | REPAROS |  |  |  |
| 4 | -CALIBRAR: AS 6- DEFLETORAS INTERNAS A ÁREA DE ESCAPE E OS CORRUGADOS. -REMOVER AGREGAÇÕES NA AREA DE ESCAPE DA TRANSITION SECTION. - DESAMASSAR ALÇA DA DOME AREA. - DESAMASSAR AREA MARCADA NA DOME AREA -CALIBRATE: THE 6- INTERNAL DEFLECTORS THE ESCAPE AREA AND THE CORRUGATED. -REMOVE AGGREGATIONS IN THE EXHAUST AREA OF THE TRANSITION SECTION. - UNCREAM HANDLE FROM THE DOME AREA. - Knead the marked area on the DOME AREA |  |  |  |  |  | REPAROS |  |  |  |
| 5 | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  | LIMPEZA |  |  |  |
| 6 | EXECUTAR FPI: ASTM E 1417, METHOD-A, LEVEL 3. APRESENTOU INDICAÇÃO? ( )SIM ( )NÃO RUN FPI: ASTM E 1417, METHOD-A, LEVEL 3. DID YOU PRESENT AN INDICATION? ( )YES ( )NO |  |  |  |  |  | NDT |  |  |  |
| 7 | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  | LIMPEZA |  |  |  |
| 8 | INSPEÇÃO FINAL. ( )APROVADO ( )REPROVADO FINAL INSPECTION. ( )APPROVED ( )FAILED |  |  |  |  |  | INSPEÇÃO |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  | ASSINATURA DO SOLICITANTE (Signature): AUGUSTO ROSA |  |  |  |  | DATA (Date): 29/11/2024 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)