| PN (PN): |  |  | SN: |  |  |  |  | Nº da OS (WO): |  |  | TLN:02623 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 23005961 |  |  | 31011 |  |  |  |  | 040607 |  |  |  |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  |  | ARTIGO/PARTE (Article/Part): |  |  | Serviço PrincipaL (Main Service) |  | QUANT: |  |  |
| EMIRADOS / CAE-550283 / TU.750236 |  |  |  | REAR BEARING SUPPORT |  |  | REVISÃO GERAL / OVERHAUL |  | 1 |  |  |
| TSN: |  |  |  | CSN: |  |  | TSO: |  | CSO: |  |  |
| ITEM (Item) | TAREFA (Task) | ETAPA (Step) |  |  | DESCRIÇÃO (Description) |  |  |  |  |  |  |
| 1 | REPAIR SHOP | SOLDAR / WELDING |  |  | PREPARAR E SOLDAR AS 4- TRINCAS NO FRONT FLANGE (REFORÇANDO OS KEY SLOTS), AS 2- NO HAT BAND E FECHAR O FURO SUPERIOR. AMS 5674 (347SS) PREPARE AND WELD THE 4- CRACKS ON THE FRONT FLANGE (REINFORCING THE KEY SLOTS), THE 2- ON THE HAT BAND AND CLOSE THE UPPER HOLE. AMS 5674 (347SS) |  |  |  |  |  |  |
| 2 | REPAIR SHOP | DESAMASSAR / SMOOTH OUT |  |  | SUAVISAR AS SOLDAS e DESOVALIZAR O FLANGE DO REAR CONE. SMOOTHING THE WELDS and DE-INSTALL THE REAR CONE FLANGE. |  |  |  |  |  |  |
| 3 | REPAIR SHOP | USINAGEM / MACHINING |  |  | USINAR OS 4- KEY SLOTS DEIXANDO: LARGURA= 0.241¨, PROFUNDIDADE= 0.120¨ e o FURO= 0.221¨, SUAVISANDO OS CANTOS VIVOS. MACHINE THE 4-KEY SLOTS LEAVING: WIDTH= 0.241 ̈, DEPTH= 0.120 ̈ and HOLE= 0.221 ̈, SMOOTHING THE SHARP CORNERS. |  |  |  |  |  |  |
| 4 | REPAIR SHOP | TRATAMENTO TERMICO / HEAT TREATMENT |  |  | TRATAMENTO TÉRMICO EM 650°C POR 3-HORAS. HEAT TREATMENT AT 650°C FOR 3-HOURS. |  |  |  |  |  |  |
| 5 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 6 | NDT | LIQUIDO PENETRANTE / FLUORESCENT PENETRANT INSPECTION |  |  | EXECUTAR FPI: ASTM E 1417, METHOD-A, LEVEL 3. APRESENTOU INDICAÇÃO? ( )SIM ( )NÃO RUN FPI: ASTM E 1417, METHOD-A, LEVEL 3. DID YOU PRESENT AN INDICATION? ( )YES ( )NO |  |  |  |  |  |  |
| 7 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 8 | T56A | INSPEÇÃO / INSPECTION |  |  | INSPEÇÃO VISUAL. VISUAL INSPECTION. |  |  |  |  |  |  |
| 9 | REPAIR SHOP | USINAGEM / MACHINING |  |  | USINAR OS DIÂMETROS ¨J e k¨ E AS FACES ¨L e M¨, DEIXANDO MUITAS MANCHAS, APENAS PARA REMOVER ALGUNS CALOS. VEJA A FIGURA ANEXA. MACHINE THE DIAMETERS ̈J and K ̈ AND the FACES ̈L and M ̈, LEAVING MANY STAINS, JUST TO REMOVE SOME CALLUSES. SEE THE ATTACHED FIGURE. |  |  |  |  |  |  |
| 10 | REPAIR SHOP | JATEAR / BLAST |  |  | APLICAR GLASS BEAD GERAL PARA CLAREAR. IP-0006, 3.26 APPLY GLASS BEAD GENERAL TO LIGHTEN. IP-0006, 3.26 |  |  |  |  |  |  |
| 11 | T56A | INSPEÇÃO / INSPECTION |  |  | INSPEÇÃO FINAL. ( )APROVADO ( )REPROVADO FINAL INSPECTION. ( )APPROVED ( )FAILED |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  | DATA (Date): |  |
|  |  |  |  |  |  | VILSON BARBOSA |  |  |  | 19/12/2024 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)