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	REGISTRO
	REVISÃO
	04

	
	RECORD
	REVISION
	

	CODIGO | CODE
	SOLICITAÇÃO DE SERVIÇOS COMPLEMENTARES
	PÁGINA
	1/1

	IAS-RG-0103
	SUPPLEMENTARY REQUEST
	PAGE
	



	PN (PN):
	SN:
	Nº da OS (WO):
	TLN:02623

	6845945
	Bl-9171
	038039
	

	Nº DO ARTIGO PRINCIPAL (Main Article):
	ARTIGO/PARTE (Article/Part):
	Serviço PrincipaL
(Main Service)
	QUANT:

	EMIRADOS  /  CAE-550502  /  Compressor
	TIE BOLT
	REVISÃO GERAL / OVERHAUL	1

	
	
	
	

	ITEM
(Item)
	[bookmark: _Hlk184222911]TAREFA
(Task)
	[bookmark: _Hlk184222919]ETAPA
(Step)
	DESCRIÇÃO
(Description)

	1
	REPAIR SHOP	DECAPAGEM / STRIPPING	REMOVER O ELECTROLESS NICKEL DOS 3 SEGUIMENTOS DO CORPO.

REMOVE THE ELECTROLESS NICKEL FROM THE 3 BODY SEGMENTS.

	2
	REPAIR SHOP	JATEAR / BLAST	ISOLAR OS RESALTOS E APLICAR GLASS BEAD NOS INTERVALOS PARA REMOVER AS CORROSÕES.   IP-0006, 3.26

ISOLATE THE BUMPS AND APPLY GLASS BEAD AT INTERVALS TO REMOVE CORROSION. IP-0006, 3.26

	3
	NDT	END- PARTICULAS MAGNETICAS / NOT - MAGNETIC PARTICLE	EXECUTAR MPI: ASTM E 1444.
APRESENTOU INDICAÇÃO? (  )SIM      (  )NÃO

RUN MPI: ASTM E 1444. DID YOU PRESENT AN INDICATION? ( )YES ( )NO

	4
	CHEMICAL CLEANING	LIMPAR / CLEAN	LIMPAR CONFORME A IP-0006, 3.10

CLEAR AS PER IP-0006, 3.10

	5
	REPAIR SHOP	DEPOSIÇÃO DE NIQUEL / NICKEL PLATING	ISOLAR OS RESALTOS, AS EXTREMIDADES E APLICAR ELECTROLESS NICKEL NOS 3- INTERVALOS DO CORPO, AMS 2404.

ISOLATE THE BUMPS, THE EXTREMITIES AND APPLY ELECTROLESS NICKEL IN THE 3-INTERVALS OF THE BODY, AMS 2404.

	6
	REPAIR SHOP	TRATAMENTO TERMICO / HEAT TREATMENT	EXECUTAR TRATAMENTO TÉRMICO EM 190° C POR 23 HORAS.

PERFORM HEAT TREATMENT AT 190° C FOR 23 HOURS.

	7
	REPAIR SHOP	FOSFATIZAÇÃO / PHOSPHATIZATION	
APLICAR PHOSPHATE AMS2404 NAS EXTREMIDADES: ROSCA E CABEÇA, VER FIGURA ANEXA.

APPLY PHOSPHATE AMS2404 TO THE ENDS: THREAD AND HEAD, SEE ATTACHED FIGURE.

	8
	T56A	INSPEÇÃO / INSPECTION	INSPEÇÃO FINAL.
(  )APROVADO         (  )REPROVADO

FINAL INSPECTION. ( )APPROVED ( )FAILED
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	OBSERVAÇÕES
(Observation):
	ASSINATURA DO SOLICITANTE 
(Signature):
	DATA 
(Date):

	[bookmark: Texto2]     
	VILSON BARBOSA
	03/01/2025


· Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.
(In case of external service, the supplier must be indicated by the purchasing department)
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