| PN (PN): |  |  | SN: |  |  |  |  | Nº da OS (WO): |  |  | TLN:02188 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 6848669 |  |  | XX11616 |  |  |  |  | IAS |  |  |  |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  |  | ARTIGO/PARTE (Article/Part): |  |  | Serviço PrincipaL (Main Service) |  | QUANT: |  |  |
| IAS / AE-108636 |  |  |  | AIR INLET HOUSING |  |  | REVISÃO GERAL / OVERHAUL |  | 1 |  |  |
| ITEM (Item) | TAREFA (Task) | ETAPA (Step) |  |  | DESCRIÇÃO (Description) |  |  |  |  |  |  |
| 1 | REPAIR SHOP | DECAPAGEM / STRIPPING |  |  | DECAPAR A TINTA, IP-0006, 3.18. PAINT STRIPPING, IP-0006, 3.18. |  |  |  |  |  |  |
| 2 | NDT | END- LIQUIDO PENETRANTE / NDT - FLUORESCENT PENETRANT INSPECTION |  |  | EXECUTAR FPI: ASTM E 1417, METHOD-A, LEVEL 3. APRESENTOU INDICAÇÃO? ( )SIM ( )NÃO RUN FPI: ASTM E 1417, METHOD-A, LEVEL 3. DID YOU PRESENT AN INDICATION? ( )YES ( )NO |  |  |  |  |  |  |
| 3 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 4 | REPAIR SHOP | ISOLAÇÃO / MASK |  |  | ISOLAR AS ROSCAS, FUROS E ÁREAS DE CONTATOS. ISOLATE THREADS, HOLES, AND CONTACT AREAS. |  |  |  |  |  |  |
| 5 | REPAIR SHOP | PINTURA / PAINTING |  |  | PINTAR EXTERNAMENTE COM: PRIMER PA-0060 e CINZA PA-0065. PAINT EXTERNALLY WITH: PRIMER PA-0060 and GRAY PA-0065. |  |  |  |  |  |  |
| 6 | REPAIR SHOP | REMOVER ISOLAMENTO / REMOVE MASK |  |  | REMOVER AS ISOLAÇÕES E OS EXCESSOS DE TINTA. REMOVE INSULATION AND EXCESS PAINT. |  |  |  |  |  |  |
| 7 | REPAIR SHOP | PINTURA / PAINTING |  |  | ISOLAR E APLICAR EMBORRACHAMENTO NO BORDO DE ATAQUE DOS STRUTS. ISOLATE AND APPLY RUBBER COATING TO THE LEADING EDGE OF THE STRUTS. |  |  |  |  |  |  |
| 8 | T56A | INSPEÇÃO / INSPECTION |  |  | SELECIONAR UM NOVO CAGE E CONFERIR O APERTO NO HOUSING. SELECT A NEW CAGE AND CHECK THE TIGHTNESS IN THE HOUSING. |  |  |  |  |  |  |
| 9 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | REMOVER O CAGE CENTRAL, ADICIONAR O NOVO E FRENA-LO COM 2- PINOS P/N= MS9105-53 REMOVE THE CENTER CAGE, ADD THE NEW ONE AND BRAKE IT WITH 2-PIN P/N= MS9105-53 |  |  |  |  |  |  |
| 10 | REPAIR SHOP | USINAGEM / MACHINING |  |  | RETIFICAR O DIÂMETRO INTERNO DO CAGE, CENTRANDO PELOS DIÂMETROS: EXTERNO CENTRAL PRÓXIMO E O EXTERNO DO ANEL GRANDE DA PERIFERIA. DEIXAR= 4.3344¨+ou- 0.0002¨ GRIND THE INNER DIAMETER OF THE CAGE, CENTERING BY THE OUTER DIAMETERS: NEAR CENTRAL OUTER AND OUTER DIAMETER OF THE LARGE PERIPHERY RING. LEAVE= 4.3344 ̈+or- 0.0002 |  |  |  |  |  |  |
| 11 | T56A | INSPEÇÃO / INSPECTION |  |  | INSPEÇÃO FINAL. ( )APROVADO ( )REPROVADO FINAL INSPECTION. ( )APPROVED ( )FAILED |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  | DATA (Date): |  |
|  |  |  |  |  |  | VILSON BARBOSA |  |  |  | 08/01/2025 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)