

	[image: Logotipo

Descrição gerada automaticamente]
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	RECORD
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	CODIGO | CODE
	SOLICITAÇÃO DE SERVIÇOS COMPLEMENTARES
	PÁGINA
	1/1

	IAS-RG-0103
	SUPPLEMENTARY REQUEST
	PAGE
	



	PN (PN):
	SN:
	Nº da OS (WO):
	TLN:02188

	6848669
	XX11616
	IAS
	

	Nº DO ARTIGO PRINCIPAL (Main Article):
	ARTIGO/PARTE (Article/Part):
	Serviço PrincipaL
(Main Service)
	QUANT:

	IAS   /   AE-108636
	AIR INLET HOUSING
	REVISÃO GERAL / OVERHAUL	1

	
	
	
	

	ITEM
(Item)
	[bookmark: _Hlk184222911]TAREFA
(Task)
	[bookmark: _Hlk184222919]ETAPA
(Step)
	DESCRIÇÃO
(Description)

	1
	REPAIR SHOP	DECAPAGEM / STRIPPING	DECAPAR A TINTA, IP-0006, 3.18.

PAINT STRIPPING, IP-0006, 3.18.

	2
	NDT	END- LIQUIDO PENETRANTE / NDT - FLUORESCENT PENETRANT INSPECTION	EXECUTAR FPI: ASTM E 1417, METHOD-A, LEVEL 3.
APRESENTOU INDICAÇÃO? (  )SIM        (  )NÃO

RUN FPI: ASTM E 1417, METHOD-A, LEVEL 3. DID YOU PRESENT AN INDICATION? ( )YES ( )NO

	3
	CHEMICAL CLEANING	LIMPAR / CLEAN	LIMPAR CONFORME A IP-0006, 3.10

CLEAR AS PER IP-0006, 3.10

	4
	REPAIR SHOP	ISOLAÇÃO / MASK	ISOLAR AS ROSCAS, FUROS E ÁREAS DE CONTATOS.

ISOLATE THREADS, HOLES, AND CONTACT AREAS.

	5
	REPAIR SHOP	PINTURA / PAINTING	PINTAR EXTERNAMENTE COM:   PRIMER PA-0060 e CINZA PA-0065.

PAINT EXTERNALLY WITH: PRIMER PA-0060 and GRAY PA-0065.

	6
	REPAIR SHOP	REMOVER ISOLAMENTO / REMOVE MASK	REMOVER AS ISOLAÇÕES E OS EXCESSOS DE TINTA.

REMOVE INSULATION AND EXCESS PAINT.

	7
	REPAIR SHOP	PINTURA / PAINTING	ISOLAR E APLICAR EMBORRACHAMENTO NO BORDO DE ATAQUE DOS STRUTS.

ISOLATE AND APPLY RUBBER COATING TO THE LEADING EDGE OF THE STRUTS.

	8
	T56A	INSPEÇÃO / INSPECTION	SELECIONAR UM NOVO CAGE E CONFERIR O APERTO NO HOUSING.

SELECT A NEW CAGE AND CHECK THE TIGHTNESS IN THE HOUSING.

	9
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	
REMOVER O CAGE CENTRAL, ADICIONAR O NOVO E FRENA-LO COM 2- PINOS P/N= MS9105-53

REMOVE THE CENTER CAGE, ADD THE NEW ONE AND BRAKE IT WITH 2-PIN P/N= MS9105-53

	10
	REPAIR SHOP	USINAGEM / MACHINING	RETIFICAR O DIÂMETRO INTERNO DO CAGE, CENTRANDO PELOS DIÂMETROS: EXTERNO CENTRAL PRÓXIMO E O EXTERNO DO ANEL GRANDE DA PERIFERIA.
DEIXAR= 4.3344¨+ou- 0.0002¨

GRIND THE INNER DIAMETER OF THE CAGE, CENTERING BY THE OUTER DIAMETERS: NEAR CENTRAL OUTER AND OUTER DIAMETER OF THE LARGE PERIPHERY RING. LEAVE= 4.3344 ̈+or- 0.0002

	11
	T56A	INSPEÇÃO / INSPECTION	INSPEÇÃO FINAL.
(  )APROVADO          (  )REPROVADO

FINAL INSPECTION. ( )APPROVED ( )FAILED
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· Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.
(In case of external service, the supplier must be indicated by the purchasing department)
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