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	REGISTRO
	REVISÃO
	04

	
	RECORD
	REVISION
	

	CODIGO | CODE
	SOLICITAÇÃO DE SERVIÇOS COMPLEMENTARES
	PÁGINA
	1/1

	IAS-RG-0103
	SUPPLEMENTARY REQUEST
	PAGE
	



	PN (PN):
	SN:
	Nº da OS (WO):
	TLN:02623

	23005961
	21988
	040117
	

	Nº DO ARTIGO PRINCIPAL (Main Article):
	ARTIGO/PARTE (Article/Part):
	Serviço PrincipaL
(Main Service)
	QUANT:

	EMIRADOS  /  TU. 750639   /   CAE-550502  /  D22A
	REAR BEARING SUPPORT
	REVISÃO GERAL / OVERHAUL	1

	
	
	
	

	ITEM
(Item)
	[bookmark: _Hlk184222911]TAREFA
(Task)
	[bookmark: _Hlk184222919]ETAPA
(Step)
	DESCRIÇÃO
(Description)

	1
	NDT	END- LIQUIDO PENETRANTE / NDT - FLUORESCENT PENETRANT INSPECTION	EXECUTAR FPI: ASTM E 1417, METHOD-A, LEVEL 3.
APRESENTOU INDICAÇÃO? (  )SIM         (  )NÃO

RUN FPI: ASTM E 1417, METHOD-A, LEVEL 3. DID YOU PRESENT AN INDICATION? ( )YES ( )NO

	2
	CHEMICAL CLEANING	LIMPAR / CLEAN	LIMPAR SEM APAGAR AS MARCAS FEITAS PELA ¨END¨
IP-0006, 3.10

CLEAR WITHOUT ERASING THE MARKS MADE BY THE ̈END ̈ IP-0006, 3.10

	3
	T56A	INSPEÇÃO / INSPECTION	INSPEÇÃO REPROGRAMAR PARA: 
FECHAR FURO SUPERIOR DA HAT BAND
REFORÇAR COM SOLDA OS SLOTS
USINAR DIÂMETROS E FACES DO FLANGE
GLASS BEAD E ¨END¨


INSPECTION RESCHEDULE TO: CLOSE TOP HOLE OF HAT BAND REINFORCING THE SLOTS WITH WELDING MACHINING FLANGE DIAMETERS AND FACES GLASS BEAD IS ̈END
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	OBSERVAÇÕES
(Observation):
	ASSINATURA DO SOLICITANTE 
(Signature):
	DATA 
(Date):

	[bookmark: Texto2]     
	VILSON BARBOSA
	10/01/2025


· Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.
(In case of external service, the supplier must be indicated by the purchasing department)
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