| PN (PN): |  |  | SN: |  |  |  |  | Nº da OS (WO): |  |  | TLN:02623 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 23061148 |  |  | WW9283 |  |  |  |  | 041259 |  |  |  |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  |  | ARTIGO/PARTE (Article/Part): |  |  | Serviço PrincipaL (Main Service) |  | QUANT: |  |  |
| EMIRADOS / CAE-550283 / D22A |  |  |  | REAR HOUSING |  |  | REVISÃO GERAL / OVERHAUL |  | 1 |  |  |
| ITEM (Item) | TAREFA (Task) | ETAPA (Step) |  |  | DESCRIÇÃO (Description) |  |  |  |  |  |  |
| 1 | REPAIR SHOP | REMOÇÃO / REMOVE |  |  | REMOVER OS PRISIONEIROS DA FRONT FACE-B. REMOVE THE PRISONERS FROM FRONT FACE-B. |  |  |  |  |  |  |
| 2 | REPAIR SHOP | USINAGEM / MACHINING |  |  | USINAR A FACE-B, SOMENTE ATÉ REMOVER A METALIZAÇÃO. MACHINE THE B-FACE, ONLY UNTIL THE METALLIZATION IS REMOVED. |  |  |  |  |  |  |
| 3 | REPAIR SHOP | ISOLAÇÃO / MASK |  |  | ISOLAR E METALIZAR A FACE-B, COM SPRA BRONZE AA VEJA A FIGURA ANEXA. ISOLATE AND METALLIZE THE B-FACE, WITH SPRA BRONZE AA SEE THE ATTACHED FIGURE. |  |  |  |  |  |  |
| 4 | REPAIR SHOP | USINAGEM / MACHINING |  |  | USINAR A METALIZAÇÃO, DEIXANDO A ALTURA TOTAL= 8.158¨+OU- 0.002¨ MACHINING THE METALLIZATION, LEAVING THE TOTAL HEIGHT = 8.158 ̈ + OR - 0.002 |  |  |  |  |  |  |
| 5 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | PREPARAR ÁREA METALIZADA: REMOVER OS EXCESSOS NAS LATERAIS, FUROS E ROSCAS. PREPARE METALLIZED AREA: REMOVE EXCESS ON THE SIDES, HOLES AND THREADS. |  |  |  |  |  |  |
| 6 | REPAIR SHOP | INSTALAR / INSTALL |  |  | INSTALAR OS PRISIONEIROS NA FACE-E. INSTALL THE STUDS ON THE E-FACE. |  |  |  |  |  |  |
| 7 | REPAIR SHOP | ISOLAÇÃO / MASK |  |  | ISOLAR AS FACES, FUROS, PRISIONEIROS E AS DEMAIS ÁREAS DE CONTATO. ISOLATE FACES, HOLES, STUDS AND OTHER CONTACT AREAS. |  |  |  |  |  |  |
| 8 | REPAIR SHOP | PINTURA / PAINTING |  |  | PINTAR EXTERNAMENTE COM: PRIME PA-0060 e CINZA PA-0065. PAINT EXTERNALLY WITH: PRIME PA-0060 and GRAY PA-0065. |  |  |  |  |  |  |
| 9 | REPAIR SHOP | REMOVER ISOLAMENTO / REMOVE MASK |  |  | REMOVER AS ISOLAÇÕES E OS EXCESSOS NOUTRAS ÁREAS. REMOVE INSULATION AND EXCESS IN OTHER AREAS. |  |  |  |  |  |  |
| 10 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR GERAL, INCLUSIVE AS VIAS INTERNAS, CONFORME A IP-0006, 3.10. CLEAN IN GENERAL, INCLUDING INTERNAL ROADS, ACCORDING TO IP-0006, 3.10. |  |  |  |  |  |  |
| 11 | T56A | INSPEÇÃO / INSPECTION |  |  | INSPEÇÃO FINAL. FINAL INSPECTION. |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  | DATA (Date): |  |
|  |  |  |  |  |  | VILSON BARBOSA |  |  |  | 13/01/2025 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)