

	[image: Logotipo

Descrição gerada automaticamente]
	REGISTRO
	REVISÃO
	04

	
	RECORD
	REVISION
	

	CODIGO | CODE
	SOLICITAÇÃO DE SERVIÇOS COMPLEMENTARES
	PÁGINA
	1/1

	IAS-RG-0103
	SUPPLEMENTARY REQUEST
	PAGE
	



	PN (PN):
	SN:
	Nº da OS (WO):
	TLN:02623

	23061148
	WW9283
	041259
	

	Nº DO ARTIGO PRINCIPAL (Main Article):
	ARTIGO/PARTE (Article/Part):
	Serviço PrincipaL
(Main Service)
	QUANT:

	EMIRADOS  /  CAE-550283   /  D22A
	REAR HOUSING
	REVISÃO GERAL / OVERHAUL	1

	
	
	
	

	ITEM
(Item)
	[bookmark: _Hlk184222911]TAREFA
(Task)
	[bookmark: _Hlk184222919]ETAPA
(Step)
	DESCRIÇÃO
(Description)

	1
	REPAIR SHOP
	REPAROS MANUAIS / MANUAL REPAIR
	PASSAR ALARGADOR DE 1.125¨+OU- 0.0005¨NOS 2- FUROS LATERAIS DOS EYE BOLTS.

PASS 1.125 ̈+OR- 0.0005 ̈REAM, IN THE 2- SIDE HOLES OF THE EYE BOLTS.

	2
	REPAIR SHOP	REMOÇÃO / REMOVE	REMOVER OS PRISIONEIROS DA FRONT FACE-B.

REMOVE THE PRISONERS FROM FRONT FACE-B.

	3
	REPAIR SHOP	USINAGEM / MACHINING	USINAR A FACE-B, SOMENTE ATÉ REMOVER A METALIZAÇÃO.

MACHINE THE B-FACE, ONLY UNTIL THE METALLIZATION IS REMOVED.

	4
	REPAIR SHOP	ISOLAÇÃO / MASK	ISOLAR E METALIZAR A FACE-B, COM SPRA BRONZE AA
VEJA A FIGURA ANEXA.

ISOLATE AND METALLIZE THE B-FACE, WITH SPRA BRONZE AA SEE THE ATTACHED FIGURE.

	5
	REPAIR SHOP	USINAGEM / MACHINING	USINAR A METALIZAÇÃO, DEIXANDO A ALTURA TOTAL= 8.158¨+OU- 0.002¨

MACHINING THE METALLIZATION, LEAVING THE TOTAL HEIGHT = 8.158 ̈ + OR - 0.002

	6
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	PREPARAR ÁREA METALIZADA:
REMOVER OS EXCESSOS NAS LATERAIS, FUROS E ROSCAS.

PREPARE METALLIZED AREA: REMOVE EXCESS ON THE SIDES, HOLES AND THREADS.

	7
	REPAIR SHOP	INSTALAR / INSTALL	INSTALAR OS PRISIONEIROS NA FACE-E.

INSTALL THE STUDS ON THE E-FACE.

	8
	REPAIR SHOP	ISOLAÇÃO / MASK	ISOLAR AS FACES, FUROS, PRISIONEIROS E AS DEMAIS ÁREAS DE CONTATO.

ISOLATE FACES, HOLES, STUDS AND OTHER CONTACT AREAS.

	9
	REPAIR SHOP	PINTURA / PAINTING	PINTAR EXTERNAMENTE COM:
PRIME PA-0060 e CINZA PA-0065.

PAINT EXTERNALLY WITH: PRIME PA-0060 and GRAY PA-0065.

	10
	REPAIR SHOP	REMOVER ISOLAMENTO / REMOVE MASK	REMOVER AS ISOLAÇÕES E OS EXCESSOS NOUTRAS ÁREAS.

REMOVE INSULATION AND EXCESS IN OTHER AREAS.

	11
	CHEMICAL CLEANING	LIMPAR / CLEAN	LIMPAR GERAL, INCLUSIVE AS VIAS INTERNAS, CONFORME A IP-0006, 3.10.

CLEAN IN GENERAL, INCLUDING INTERNAL ROADS, ACCORDING TO IP-0006, 3.10.

	12
	T56A	INSPEÇÃO / INSPECTION	INSPEÇÃO FINAL.

FINAL INSPECTION.
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· Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.
(In case of external service, the supplier must be indicated by the purchasing department)
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