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	DESCRIÇÃO
(Description)

	1
	REPAIR SHOP	REMOÇÃO / REMOVE	     REMOVER O CAGE CENTRAL, LIMPAR CONTATOS E REINSTALA-LO ( PODE PASSAR ¨PEQUENA¨ PELÍCULA DE COLA)

REMOVE THE CENTRAL CAGE, CLEAN CONTACTS AND REINSTALL IT (CAN PASS "SMALL" GLUE FILM)

	2
	REPAIR SHOP	REMOÇÃO / REMOVE	REMOVER O CAGE MENOR E SEUS PRISIONEIROS (DO PINION).

REMOVE THE SMALLER CAGE AND ITS STUDS (FROM THE PINION).

	3
	REPAIR SHOP	USINAGEM / MACHINING	USINAR TODA FACE-D, ATÉ REMOVER A METALIZAÇÃO.

MACHINE THE ENTIRE D-FACE, UNTIL THE METALLIZATION IS REMOVED.

	4
	REPAIR SHOP	METALIZAÇÃO / THERMAL SPRAY	ISOLAR E METALIZAR TODA FACE-D, COM SPRA BRONZE AA.
VEJA A FIGURA ANEXA.

ISOLATE AND METALLIZE THE ENTIRE D-FACE, WITH SPRA BRONZE AA. SEE THE ATTACHED FIGURE.

	5
	REPAIR SHOP	USINAGEM / MACHINING	APOIAR NA MESA A FACE-C EM 4 PONTOS E USINAR A METALIZAÇÃO, DEIXANDO A ESPESSURA= 0.875¨+OU- 0.002¨e a DIMENÇÃO-A= 0.345¨ +OU- 0.004¨

REST THE C-FACE ON THE TABLE AT 4 POINTS AND MACHINE THE METALLIZATION, LEAVING THE THICKNESS = 0.875 ̈ + OR- 0.002 ̈ and the DIMENSION-A = 0.345 ̈ +OR- 0.004

	6
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	PREPARAR SUAVISANDO A ÁREA METALIZADA, REMOVENDO OS EXCESSOS DAS PROXIMIDADES E DOS FUROS.
Nota: Pegar outro modelo para verificar onde tem rebaixos, 2-furos de lubrificação e roscas.

PREPARE YOUR VIEW OF THE METALLIZED AREA, REMOVING EXCESS FROM THE VICINITY AND HOLES. Note: Take another model to check where it has undercuts, 2-hole lubrication and threads.

	7
	REPAIR SHOP	INSTALAR / INSTALL	INSTALAR OS 7- PRISIONEIROS, O CAGE E AS NUTS.

INSTALL THE 7- PRISONERS, THE CAGE AND THE NUTS.

	8
	REPAIR SHOP	ISOLAÇÃO / MASK	ISOLAR AMBOS OS LADOS PARA PINTAR A PERIFERIA.

ISOLATE BOTH SIDES TO PAINT THE PERIPHERY.

	9
	REPAIR SHOP	PINTURA / PAINTING	PINTAR A PERIFERIA COM PRIMER PA-0060 e CINZA PA-0065.

PAINT THE PERIPHERY WITH PRIMER PA-0060 and GRAY PA-0065.

	10
	CHEMICAL CLEANING	LIMPAR / CLEAN	LIMPAR CONFORME A IP-0006, 3.10.

CLEAR AS PER IP-0006, 3.10.

	11
	T56A	INSPEÇÃO / INSPECTION	INSPEÇÃO FINAL.

FINAL INSPECTION.
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· Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.
(In case of external service, the supplier must be indicated by the purchasing department)
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