| PN (PN): |  |  | SN: |  |  |  |  | Nº da OS (WO): |  |  | TLN: |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 23058707 |  |  | AAA8073 |  |  |  |  | 039829 |  |  |  |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  |  | ARTIGO/PARTE (Article/Part): |  |  | Serviço PrincipaL (Main Service) |  | QUANT: |  |  |
| AE-109020 |  |  |  | COMBUSTION LINER ASSY |  |  | REVISÃO GERAL / OVERHAUL |  | 01 |  |  |
| TSN: |  |  |  | CSN: |  |  | TSO: |  | CSO: |  |  |
| ITEM (Item) | TAREFA (Task) | ETAPA (Step) |  |  | DESCRIÇÃO (Description) |  |  |  |  |  |  |
| 1 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | DESAMASSAR AS AREAS MARCADAS COM PINCEL AZUL, NA DOME AREA. REMOVE AREAS MARKED WITH A BLUE BRUSH, IN THE DOME AREA |  |  |  |  |  |  |
| 2 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | CALIBRAR OS CORRUGADOS. CALIBRATE THE CORRUGATES. |  |  |  |  |  |  |
| 3 | REPAIR SHOP | SOLDAR / WELDING |  |  | SOLDAR TRINCA INTERNA MARCADA DE PINCEL AZUL NA AREA DE ESCAPE DA TRANSITION. AMS-5798 WELD INTERNAL CRACK MARKED WITH A BLUE BRUSH IN THE EXHAUST AREA OF THE TRANSITION. AMS-5798 |  |  |  |  |  |  |
| 4 | REPAIR SHOP | TRATAMENTO TERMICO / HEAT TREATMENT |  |  | EXECUTAR TRATAMENTO TÉRMICO EM 1010°C, POR 30 MINUTOS. PERFORM HEAT TREATMENT AT 1010°C FOR 30 MINUTES. |  |  |  |  |  |  |
| 5 | T56A | INSPEÇÃO / INSPECTION |  |  | INSPEÇÃO VISUAL. VISUAL INSPECTION. |  |  |  |  |  |  |
| 6 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.1 |  |  |  |  |  |  |
| 7 | NDT | END- LIQUIDO PENETRANTE / NDT - FLUORESCENT PENETRANT INSPECTION |  |  | EXECUTAR FPI: ASTM E 1417, METHOD-A, LEVEL 3. APRESENTOU INDICAÇÃO? ( )SIM ( )NÃO RUN FPI: ASTM E 1417, METHOD-A, LEVEL 3. DID YOU PRESENT AN INDICATION? ( )YES ( )NO |  |  |  |  |  |  |
| 8 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.1 |  |  |  |  |  |  |
| 9 | T56A | INSPEÇÃO / INSPECTION |  |  | INSPEÇÃO FINAL. ( )APROVADO ( )REPROVADO FINAL INSPECTION. ( )APPROVED ( )FAILED |  |  |  |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  | DATA (Date): |  |
|  |  |  |  |  |  | AUGUSTO ROSA |  |  |  | 20/01/2025 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)