| PN (PN): |  |  | SN: |  |  |  |  | Nº da OS (WO): |  |  | TLN: |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 6788710 |  |  | N/A |  |  |  |  | 039503 |  |  | 02686 |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  |  | ARTIGO/PARTE (Article/Part): |  |  | Serviço PrincipaL (Main Service) |  | QUANT: |  |  |
| AE-106837 |  |  |  | BODY ASSY, PRESSURE & SCAVENGE OIL PUMP |  |  | REPARO T56 / REPAIR T56 |  | 4 EA |  |  |
| TSN: |  |  |  | CSN: |  |  | TSO: |  | CSO: |  |  |
| ITEM (Item) | TAREFA (Task) | ETAPA (Step) |  |  | DESCRIÇÃO (Description) |  |  |  |  |  |  |
| 1 | CHEMICAL CLEANING | DECAPAGEM/ DECAPPING |  |  | Realizar remoção do coating remanescente conforme SPOP 260 (IAS-IP-0006 3.18 Rev.3). Do stripping remaning coating per SPOP 260 (IAS-IP-0006 3.18 Rev.3). |  |  |  |  |  |  |
|  | NDT | LIQUIDO PENETRANTE |  |  | Realizar FPI conforme TASK 70-21-01-200-801, Norma AMS 2644, ASTM E 1417 em todas as áreas Perform FPI according to TASK 70-21-01-200-801, AMS Standard 2644, ASTM E 1417 in all areas |  |  |  |  |  |  |
|  | CHEMICAL CLEANING | LIMPEZA / CLEAN |  |  | Limpeza pós NDT conforme IP-0006 PAR 3.34 Clean post NDT per IP-0006 PAR 3.34 |  |  |  |  |  |  |
|  | PAITING | ISOLAÇÃO / MASK |  |  | Isole faces de contato, pinos, furos e sleeves Insulate contact faces, pins, holes and sleevs |  |  |  |  |  |  |
| 2 | PAITING | PINTURA / PAITING |  |  | Aplicar Primer PA0060, em seguida aplicar PA0065 CINZA INLET Apply Primer PA0060, then apply gray inlet PA0065 |  |  |  |  |  |  |
| 3 | PAITING | REMOÇÃO / REMOVE |  |  | Remova isolações e certifique-se que o coating está aplicado corretamente na peça e de que o local onde foi aplicado o coating esteja uniforme e com um bom acabamento. Remove mask from the part and do check of the coating for full coverage. Make sure the finished coating has a smooth surface. |  |  |  |  |  |  |
|  | T56 | INSPEÇÃO / INSPECTION |  |  | Inspeção final. Final inspection. |  |  |  |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  | DATA (Date): |  |
| TAG’S: 0011494 / 0011495 / 001493 / 0011492 |  |  |  |  |  | Pedro Fonseca |  |  |  | 27/01/2025 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)