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	REGISTRO
	REVISÃO
	04

	
	RECORD
	REVISION
	

	CODIGO | CODE
	SOLICITAÇÃO DE SERVIÇOS COMPLEMENTARES
	PÁGINA
	1/1

	IAS-RG-0103
	SUPPLEMENTARY REQUEST
	PAGE
	



	PN (PN):
	SN:
	Nº da OS (WO):
	TLN:

	6846213
	N/A
	039503
	02686

	Nº DO ARTIGO PRINCIPAL (Main Article):
	ARTIGO/PARTE (Article/Part):
	Serviço PrincipaL
(Main Service)
	QUANT:

	AE-106837

	FITTING ASSY, VENT, FLANGED
	REPARO T56 / REPAIR T56	3 EA

	TSN:
	CSN:
	TSO:
	CSO:

	ITEM
(Item)
	[bookmark: _Hlk184222911]TAREFA
(Task)
	[bookmark: _Hlk184222919]ETAPA
(Step)
	DESCRIÇÃO
(Description)

	
	CHEMICAL CLEANING	LIMPEZA / CLEAN
	Realizar limpeza conforme SPOP 209.

Relize Clean per SPOP 209.

	1
	NDT
	LIQUIDO PENETRANTE 
	Realizar FPI conforme TASK 70-21-01-200-801, Norma AMS 2644, ASTM E 1417 em todas as áreas

Perform FPI according to TASK 70-21-01-200-801, AMS Standard 2644, ASTM E 1417 in all areas

	2
	CHEMICAL CLEANING	LIMPEZA / CLEAN
	Limpeza pós NDT conforme IP-0006 PAR 3.34

Clean post NDT per IP-0006 PAR 3.34

	3
	PAITING
	ISOLAÇÃO / MASK
	Isole faces de contato, pinos, furos e sleeves

Insulate contact faces, pins, holes and sleevs

	4
	PAITING
	PINTURA / PAITING
	Aplicar Primer PA0060, em seguida aplicar PA0065 CINZA INLET

Apply Primer PA0060, then apply gray inlet PA0065


	5
	PAITING
	REMOÇÃO /  REMOVE
	Remova isolações e certifique-se que o coating está aplicado corretamente na peça e de que o local onde foi aplicado o coating esteja uniforme e com um bom acabamento.

Remove mask from the part and do check of the coating for full coverage. Make sure the finished coating has a smooth surface.

	6
	T56
	INSPEÇÃO /  INSPECTION
	Inspeção final.

Final inspection.

	OBSERVAÇÕES
(Observation):
	ASSINATURA DO SOLICITANTE 
(Signature):
	DATA 
(Date):

	TAG’S: 0011469 / 0011457 / 0011456 
	Pedro Fonseca
	27/01/2025

	
	
	


· Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.
(In case of external service, the supplier must be indicated by the purchasing department)
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