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	REGISTRO
	REVISÃO
	04

	
	RECORD
	REVISION
	

	CODIGO | CODE
	SOLICITAÇÃO DE SERVIÇOS COMPLEMENTARES
	PÁGINA
	1/1

	IAS-RG-0103
	SUPPLEMENTARY REQUEST
	PAGE
	



	PN (PN):
	SN:
	Nº da OS (WO):
	TLN:

	6894131
	VIDE OBS:
	39484
	02623

	Nº DO ARTIGO PRINCIPAL (Main Article):
	ARTIGO/PARTE (Article/Part):
	Serviço PrincipaL
(Main Service)
	QUANT:

	CAE-550449
	PLANET BEARING SEPARATORS
	REVISÃO GERAL / OVERHAUL	10 EA

	TSN:
	CSN:
	TSO:
	CSO:

	ITEM
(Item)
	[bookmark: _Hlk184222911]TAREFA
(Task)
	[bookmark: _Hlk184222919]ETAPA
(Step)
	DESCRIÇÃO
(Description)

	1
	CHEMICAL CLEANING	DEPOSIÇÃO DE PRATA/ SILVER PLATING	REALIZAR A REMOÇÃO DE PRATA NOS SEPARADORES.

REMOVE SILVER IN THE SEPARATORS

	2
	CHEMICAL CLEANING	PARTICULA MAGNETICA / MAGNETIC PARTICLE	EXECUTAR MPI CONFORME OHM 4RC3 TASK 70-21-03-200-801, REFERENCIA NORMA ASTM E1444.

PERFORM MPI ACCORDING TO OHM 4RC3 TASK 70-21-03-200-801, REFERENCE ASTM STANDARD E1444.

FORAM ENCONTRADAS INDICAÇÕES?
WERE INDICATIONS FOUND?
(   )SIM/YES 
(   )NÃO/NO

	3
	NDT	LIQUIDO PENETRANTE / FLUORESCENT PENETRANT INSPECTION	REALIZAR NDT NOS SEPARADORES CONFORME:
ENSAIO: FPI ASTM E 14417
MÉTODO: D
SENSIBILIDADE: 4

APRESENTOU INDICAÇÕES? (  )SIM (  )NÃO, PROSSIGA COM A ETAPA DE LIMPEZA PÓS-NDT.

PERFORM NDT IN TH SEPARATORS CONFORM:
TEST:  FPI ASTM E 14417
METHOD: D
SENSIBILITY: 4

DID YOU FOUND ANY INDICATIONS? (  )YES  (  )NO, PROCEED TO THE POST NDT CLEANING STEP.

	4
	CHEMICAL CLEANING	LIMPAR / CLEAN	REALIZAR LIMPEZA PÓS NDT CONFORME IP-006, ITEM 3.34.

PERFORM POST-NDT CLEANING IN ACCORDANCE WITH IP-006, ITEM 3.34.

	5
	T56A	INSPEÇÃO / INSPECTION	REALIZAR INSPEÇÃO APÓS OPERAÇÃO DE MPI.
PERFORM INSPECTION AFTER FPI OPERATION.

REFIRA-SE AOS RESULTADOS REGISTRADOS NO IAS RG-0332 (CASO TENHA) E PREENCHER O MESMO COM DEVIDAS OBSERVAÇÕES.
REFER TO THE RESULTS RECORDED IN IAS RG-0332( IF ANY) AND FILL IT OUT WITH APPROPRIATE OBSERVATIONS.

AVALIAR OS LIMITES SE ACEITAÇÃO CONFORME OHM
EVALUATE THE LIMITS OF ACCEPTANCE ACCORDING TO OHM.


(   )APROVADO, APPROVED
(   )REJEITADO, REJECTED

ANEXAR E REGISTRAR N° LAUDO NDT: _______________
ATTACH AND REGISTER NDT REPORT NO.


	6
	CHEMICAL CLEANING	DEPOSIÇÃO DE PRATA/ SILVER PLATING	REALIZAR BANHO DE PRATA NOS SEPARADORES CONFORME AMS 2412.

APLLY SILVER PLATING IN THE SEPARATORS CONFORME AMS 2412.

	7
	T56A	APROVAÇÃO FINAL DO SERVLÇO REALIZADO / FINAL APPROVAL OF THE SERVICE	REALIZAR INSPEÇÃO FINAL

PERFORM FINAL INSPECTION

(   )APROVADO, APPROVED
(   )REJEITADO, REJECTED



	OBSERVAÇÕES
(Observation):
	ASSINATURA DO SOLICITANTE 
(Signature):
	DATA 
(Date):

	
MOTOR : CAE-550449

SEPARADORES:

S/N: ND126RR   QTD: 02EA
S/N: ND121RR   QTD: 02EA
S/N: ND161RR   QTD: 02EA
S/N: ND165RR   QTD: 02EA
S/N: ND160RR   QTD: 02EA

	AUGUSTO ROSA
	11/02/2025


· Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.
(In case of external service, the supplier must be indicated by the purchasing department)
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