| PN (PN): |  |  | SN: |  |  |  |  | Nº da OS (WO): |  |  | TLN:02188 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 6871447 |  |  | 16385 |  |  |  |  | ias |  |  |  |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  |  | ARTIGO/PARTE (Article/Part): |  |  | Serviço PrincipaL (Main Service) |  | QUANT: |  |  |
| IAS / AE-109024 / -15 |  |  |  | COMPRESSOR CASE |  |  | REVISÃO GERAL / OVERHAUL |  | 1 |  |  |
| ITEM (Item) | TAREFA (Task) | ETAPA (Step) |  |  | DESCRIÇÃO (Description) |  |  |  |  |  |  |
| 1 | CHEMICAL CLEANING | JATEAR / BLAST |  |  | APLICAR GLASS BEAD EXTERNAMENTE PARA LIMPAR, IP-0006, 3.26 APPLY GLASS BEAD EXTERNALLY FOR LIMPAR, IP-0006, 3.26 |  |  |  |  |  |  |
| 2 | NDT | END- LIQUIDO PENETRANTE / NDT - FLUORESCENT PENETRANT INSPECTION |  |  | EXECUTAR FPI: ASTM E 1417, METHOD-A, LEVEL 3. APRESENTOU INDICAÇÃO? ( )SIM ( )NÃO CASO POSITIVO, DEVOLVA PARA INSPEÇÃO. RUN FPI: ASTM E 1417, METHOD-A, LEVEL 3. DID YOU PRESENT AN INDICATION? ( )YES ( )NO IF SO, RETURN FOR INSPECTION. |  |  |  |  |  |  |
| 3 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP- 0006, 3.10. CLEAR ACCORDING TO IP-0006, 3.10. |  |  |  |  |  |  |
| 4 | REPAIR SHOP | ISOLAÇÃO / MASK |  |  | ISOLAR FUROS, PRISIONEIROS E ÁREAS DE CONTATO. ISOLATE HOLES, STUDS, AND CONTACT AREAS. |  |  |  |  |  |  |
| 5 | REPAIR SHOP | PINTURA / PAINTING |  |  | APLICAR SERMETEL EXTERNAMENTE, CONFORME A IP-0006, 3.17 APPLY SERMETEL EXTERNALLY, IN ACCORDANCE WITH IP-0006, 3.17 |  |  |  |  |  |  |
| 6 | REPAIR SHOP | REMOVER ISOLAMENTO / REMOVE MASK |  |  | REMOVER AS ISOLAÇÕES E OS EXCESSOS DE SERMETEL. REMOVE INSULATION AND EXCESS FROM SERMETEL. |  |  |  |  |  |  |
| 7 | REPAIR SHOP | METALIZAÇÃO / THERMAL SPRAY |  |  | ISOLAR E METALIZAR INTERNAMENTE COM ALUMÍNIO . INSULATE AND METALLIZE INTERNALLY WITH ALUMINUM. |  |  |  |  |  |  |
| 8 | REPAIR SHOP | USINAGEM / MACHINING |  |  | USINAR AS CANALETAS CONFORME A FIGURA ANEXA. VEJA A FIGURA ANEXA. MACHINE THE GUTTERS ACCORDING TO THE ATTACHED FIGURE. SEE THE ATTACHED FIGURE. |  |  |  |  |  |  |
| 9 | REPAIR SHOP | USINAGEM / MACHINING |  |  | USINAR OS DIÂMETROS INTERNOS COM ALUMÍNIO. DEIXAR DO 1º ao 9º ST= ……………….. DEIXAR DO 10º ao 14º ST= …………….. VEJA A FIGURA ANEXA. MACHINE THE INNER DIAMETERS WITH ALUMINUM. LEAVE FROM 1st to 9th ST= .................... LEAVE FROM 10th to 14th ST= ................. SEE THE ATTACHED FIGURE. |  |  |  |  |  |  |
| 10 | REPAIR SHOP | USINAGEM / MACHINING |  |  | USINAR OS CHANFROS, CONFORME A FIGURA ANEXA. MACHINE THE CHAMFERS, AS SHOWN IN THE ATTACHED FIGURE. |  |  |  |  |  |  |
| 11 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | PREPARAR AS ÁREAS USINADAS, POLIR AS FACES E ROSCAS. PREPARE THE MACHINED AREAS, POLISH THE FACES AND THREADS. |  |  |  |  |  |  |
| 12 | REPAIR SHOP | MONTAG EM/ ASSEMBLY |  |  | MONTAR E ALINHAR AS VANES, CONFORME A FIGURA ANEXA. ASSEMBLE AND ALIGN THE VANES, AS SHOWN IN THE ATTACHED FIGURE. |  |  |  |  |  |  |
| 13 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | REMOVER OS EXCESSOS SE TIVER NOS COMPRIMENTOS DOS ARCOS, QUE ESTIVEREM SALIENTES ÀS FACES DO CASING. REMOVE THE EXCESS IF THERE IS IN THE LENGTHS OF THE ARCHES, WHICH ARE PROTRUDING FROM THE CASING FACES. |  |  |  |  |  |  |
| 14 | REPAIR SHOP | USINAGEM / MACHINING |  |  | USINAR O DIÂMETRO INTERNO DOS 26- SEALS, CONFORME A FIGURA ANEXA. MACHINE THE INTERNAL DIAMETER OF THE 26-SEALS, AS SHOWN IN THE ATTACHED FIGURE. |  |  |  |  |  |  |
| 15 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10. CLEAR AS PER IP-0006, 3.10. |  |  |  |  |  |  |
| 16 | T56A | INSPEÇÃO / INSPECTION |  |  | INSPEÇÃO FINAL. ( )APROVADO ( )REPROVADO FINAL INSPECTION. ( )APPROVED ( )FAILED |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  | DATA 11/02/2025 (Date): |  |
|  |  |  |  |  |  | VILSON BARBOSA |  |  |  | 11/02/2025 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)