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	Nº DO ARTIGO PRINCIPAL (Main Article):
	ARTIGO/PARTE (Article/Part):
	Serviço PrincipaL
(Main Service)
	QUANT:

	IAS  /  AE-109024  /  -15
	                 COMPRESSOR CASE
	REVISÃO GERAL / OVERHAUL	1

	
	
	
	

	ITEM
(Item)
	[bookmark: _Hlk184222911]TAREFA
(Task)
	[bookmark: _Hlk184222919]ETAPA
(Step)
	DESCRIÇÃO
(Description)

	1
	CHEMICAL CLEANING	JATEAR / BLAST	APLICAR GLASS BEAD EXTERNAMENTE PARA LIMPAR, IP-0006, 3.26

APPLY GLASS BEAD EXTERNALLY FOR LIMPAR, IP-0006, 3.26

	2
	NDT	END- LIQUIDO PENETRANTE / NDT - FLUORESCENT PENETRANT INSPECTION	EXECUTAR FPI: ASTM E 1417, METHOD-A, LEVEL 3.
APRESENTOU INDICAÇÃO? (  )SIM     (  )NÃO
CASO POSITIVO, DEVOLVA PARA INSPEÇÃO.

RUN FPI: ASTM E 1417, METHOD-A, LEVEL 3. DID YOU PRESENT AN INDICATION? ( )YES ( )NO IF SO, RETURN FOR INSPECTION.

	3
	CHEMICAL CLEANING	LIMPAR / CLEAN	LIMPAR CONFORME A IP- 0006, 3.10.

CLEAR ACCORDING TO IP-0006, 3.10.

	4
	REPAIR SHOP	ISOLAÇÃO / MASK	ISOLAR FUROS, PRISIONEIROS E ÁREAS DE CONTATO.

ISOLATE HOLES, STUDS, AND CONTACT AREAS.

	5
	REPAIR SHOP	PINTURA / PAINTING	APLICAR SERMETEL EXTERNAMENTE, CONFORME A IP-0006, 3.17

APPLY SERMETEL EXTERNALLY, IN ACCORDANCE WITH IP-0006, 3.17

	6
	REPAIR SHOP	REMOVER ISOLAMENTO / REMOVE MASK	REMOVER AS ISOLAÇÕES E OS EXCESSOS DE SERMETEL.

REMOVE INSULATION AND EXCESS FROM SERMETEL.

	7
	REPAIR SHOP	METALIZAÇÃO / THERMAL SPRAY	ISOLAR E METALIZAR INTERNAMENTE COM ALUMÍNIO .

INSULATE AND METALLIZE INTERNALLY WITH ALUMINUM.

	8
	REPAIR SHOP	USINAGEM / MACHINING	USINAR AS CANALETAS CONFORME A FIGURA ANEXA.
VEJA A FIGURA ANEXA.

MACHINE THE GUTTERS ACCORDING TO THE ATTACHED FIGURE. SEE THE ATTACHED FIGURE.

	9
	REPAIR SHOP	USINAGEM / MACHINING	USINAR OS DIÂMETROS INTERNOS COM ALUMÍNIO.
DEIXAR DO 1º ao 9º ST= ………………..
DEIXAR DO 10º ao 14º ST= ……………..
VEJA A FIGURA ANEXA.

MACHINE THE INNER DIAMETERS WITH ALUMINUM. LEAVE FROM 1st to 9th ST= .................... LEAVE FROM 10th to 14th ST= ................. SEE THE ATTACHED FIGURE.

	10
	REPAIR SHOP	USINAGEM / MACHINING	USINAR OS CHANFROS, CONFORME A FIGURA ANEXA.

MACHINE THE CHAMFERS, AS SHOWN IN THE ATTACHED FIGURE.

	11
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	PREPARAR AS ÁREAS USINADAS, POLIR AS FACES E ROSCAS.

PREPARE THE MACHINED AREAS, POLISH THE FACES AND THREADS.

	12
	REPAIR SHOP	MONTAG EM/ ASSEMBLY	MONTAR E ALINHAR AS VANES, CONFORME A FIGURA ANEXA.

ASSEMBLE AND ALIGN THE VANES, AS SHOWN IN THE ATTACHED FIGURE.

	13
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	REMOVER OS EXCESSOS SE TIVER NOS COMPRIMENTOS DOS ARCOS, QUE ESTIVEREM SALIENTES ÀS FACES DO CASING.

REMOVE THE EXCESS IF THERE IS IN THE LENGTHS OF THE ARCHES, WHICH ARE PROTRUDING FROM THE CASING FACES.

	14
	REPAIR SHOP	USINAGEM / MACHINING	USINAR O DIÂMETRO INTERNO DOS 26- SEALS, CONFORME A FIGURA ANEXA.

MACHINE THE INTERNAL DIAMETER OF THE 26-SEALS, AS SHOWN IN THE ATTACHED FIGURE.

	15
	CHEMICAL CLEANING	LIMPAR / CLEAN	LIMPAR CONFORME A IP-0006, 3.10.

CLEAR AS PER IP-0006, 3.10.

	16
	T56A	INSPEÇÃO / INSPECTION	INSPEÇÃO FINAL.
(  )APROVADO         (  )REPROVADO

FINAL INSPECTION. ( )APPROVED ( )FAILED

	
	Escolher um item.	Escolher um item.	

	
	Escolher um item.	Escolher um item.	

	
	Escolher um item.	Escolher um item.	

	
	Escolher um item.	Escolher um item.	

	
	Escolher um item.	Escolher um item.	

	
	Escolher um item.	Escolher um item.	
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(Observation):
	ASSINATURA DO SOLICITANTE 
(Signature):
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	VILSON BARBOSA
	11/02/2025


· Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.
(In case of external service, the supplier must be indicated by the purchasing department)
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