| PN (PN): |  |  | SN: |  |  |  |  | Nº da OS (WO): |  |  | TLN: |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| VIDE OBS |  |  | VIDE OBS |  |  |  |  | 39484 |  |  | 02188 |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  |  | ARTIGO/PARTE (Article/Part): |  |  | Serviço PrincipaL (Main Service) |  | QUANT: |  |  |
| CAE- 550449 |  |  |  | BEARING SEPARATOR |  |  | REVISÃO GERAL / OVERHAUL |  | 01 |  |  |
| TSN: |  |  |  | CSN: |  |  | TSO: |  | CSO: |  |  |
| ITEM (Item) | TAREFA (Task) | ETAPA (Step) |  |  | DESCRIÇÃO (Description) |  |  |  |  |  |  |
| 1 | CHEMICAL CLEANING | REMOÇÃO / REMOVE |  |  | REMOVER O BANHO DE PRATA. OBS: PEÇA DE BRONZE REMOVE THE SILVER PLATE. NOTE: BRONZE PIECE |  |  |  |  |  |  |
| 2 | NDT | NON-DESTRUCTIVE TESTING |  |  | EXECUTAR FPI: ASTM E 1417, METHOD-D, LEVEL-4. FORAM ENCONTRADAS INDICAÇÕES? ( ) SIM ( )NÃO RUN FPI: ASTM E 1417, METHOD-D, LEVEL-4. WERE INDICATIONS FOUND? ( ) YES ( )NO |  |  |  |  |  |  |
| 3 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 4 | CHEMICAL CLEANING | DEPOSIÇÃO DE PRATA/ SILVER PLATING |  |  | APLICAR BANHO DE PRATA, COM O DOBRO DO TEMPO USADO EM PARAFUSOS. IT-0279 APPLY SILVER PLATING, TWICE AS LONG AS USED ON SCREWS. IT-0279 |  |  |  |  |  |  |
| 5 | T56A | INSPEÇÃO / INSPECTION |  |  | INSPEÇÃO FINAL. ( )APROVADO ( )REPROVADO FINAL INSPECTION. ( )APPROVED ( )FAILED |  |  |  |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  | DATA (Date): |  |
| P/N----------S/N-------- 6890541 ND9185 23062205 JJ13244 6876006 GGA856 23055591 JJ04911 6845263 ND828Y 6844090 ND3864 6878485 MP44573 23062205 JJ13240 6825699 GG091A 6878485 MP45487 6829374 GG38028 23062205 JJ13213 23062238 JJ02214 6878485 MP44769 6878485 MP48708 6825802 GG9379 6829374 GG38033 23064888 JJ05072 6878485 MP45430 6878485 MP48759 6845263 ND813Y 23003208 ND0960 6873232 GGE833 6829354 ND990A |  |  |  |  |  | AUGUSTO ROSA |  |  |  | 13/02/2025 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)