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	SOLICITAÇÃO DE SERVIÇOS COMPLEMENTARES
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	PN (PN):
	SN:
	Nº da OS (WO):
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	Nº DO ARTIGO PRINCIPAL (Main Article):
	ARTIGO/PARTE (Article/Part):
	Serviço PrincipaL
(Main Service)
	QUANT:

	EMIRADOS  /  CAE-550283  /  D22A
	1- ACCESSORY BOX HOUSING
	REVISÃO GERAL / OVERHAUL	1

	
	
	
	

	ITEM
(Item)
	[bookmark: _Hlk184222911]TAREFA
(Task)
	[bookmark: _Hlk184222919]ETAPA
(Step)
	DESCRIÇÃO
(Description)

	1
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	ABRIR MAIS A TRINCA NAS DUAS ÁREAS INTERNAS, PARA EFETUAR A SOLDA.

OPEN THE CRACK MORE IN THE TWO INTERNAL AREAS, TO PERFORM THE WELDING.

	2
	REPAIR SHOP	SOLDAR / WELDING	ENCHER COM SOLDA AS DUAS ÁREAS BLENDADAS.
USAR: MIL-R-6944, grade B, AZ-101 magnesium alloy welding rod.

FILL THE TWO BLENDED AREAS WITH SOLDER. USE: MIL-R-6944, grade B, AZ-101 magnesium alloy welding rod.

	3
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	PREPARAR AS SOLDAS DEIXANDO NO FORMATO ORIGINAL E POLIR.

PREPARE THE WELDS LEAVING THEM IN THEIR ORIGINAL SHAPE AND POLISH.

	4
	REPAIR SHOP	TRATAMENTO TERMICO / HEAT TREATMENT	EXECUTAR ALÍVIO DE TENÇÃO EM 190°C POR 4- HORAS.

PERFORM STRAIN RELIEF AT 190°C FOR 4-HOURS.

	5
	CHEMICAL CLEANING	LIMPAR / CLEAN	LIMPAR CONFORME A IP-0006, 3.10

CLEAR AS PER IP-0006, 3.10

	6
	NDT	END- LIQUIDO PENETRANTE / NDT - FLUORESCENT PENETRANT INSPECTION	EXECUTAR FPI: ASTM E 1417, METHOD-A, LEVEL 3.
APRESENTOU INDICAÇÃO? (  )SIM       (  )NÃO
NOTA: CASO POSITIVO, ENTREGAR PARA INSPEÇÃO.

RUN FPI: ASTM E 1417, METHOD-A, LEVEL 3. DID YOU PRESENT AN INDICATION? ( )YES ( )NO NOTE: IF SO, SUBMIT FOR INSPECTION.

	7
	CHEMICAL CLEANING	LIMPAR / CLEAN	LIMPAR CONFORME A IP-0006, 3.10

CLEAR AS PER IP-0006, 3.10

	8
	REPAIR SHOP	ISOLAÇÃO / MASK	ISOLAR OS FUROS, PRISIONEIROS E ÁREAS DE CONTATO.

ISOLATE THE HOLES, STUDS AND CONTACT AREAS.

	9
	REPAIR SHOP	PINTURA / PAINTING	PINTAR EXTERNAMENTE COM:
PRIME PA-0060  e  CINZA PA-0065.

PAINT EXTERNALLY WITH: PRIME PA-0060 and GRAY PA-0065.

	10
	T56A	INSPEÇÃO / INSPECTION	INSPEÇÃO FINAL.
(  )APROVADO          (  )REPROVADO

FINAL INSPECTION. ( )APPROVED ( )FAILED
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	DATA 25/02/2025
(Date):

	[bookmark: Texto2]     
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· Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.
(In case of external service, the supplier must be indicated by the purchasing department)
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