| PN (PN): |  | SN: |  |  |  | Nº da OS (WO): |  |  |  | TLN: |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| RR30000522 |  | YP11860 |  |  |  | 043139 |  |  |  | 02027 |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  | ARTIGO/PARTE (Article/Part): |  |  |  |  | QUANT: |  |  |
| RRE-200279 |  |  | Gearbox cover |  |  |  |  | 01 EA |  |  |
| TSN: N/A |  |  | CSN: N/A |  | TSO: N/A |  |  | CSO: N/A |  |  |
| ITEM (Item) | DESCRIÇÃO DO SERVIÇO A EXECUTAR (Description of the work to be executed) |  |  |  |  |  | EXECUÇÃO (Execution) |  |  | *SETOR/FORNECEDOR (Sector/Supplier) |
|  | Service requested: Treat corrosion and restore coating per HMM CSP22005. |  |  |  |  |  |  |  |  |  |
|  | Remover coating conforme SPM CSP22006 Task 70-34-07-300-801. Remove coating per SPM CSP22006 Task 70-34-07-300-801. |  |  |  |  |  |  |  |  | LIMPEZA QUÍMICA |
|  | Realizar inspeção na tridimencional e anexar laudo assinado. Carry out a three-dimensional inspection and attach a signed report. |  |  |  |  |  |  |  |  | TRIDIMENCIONAL |
|  | Remover corrosão nas superfícies externas, aplicar epoxy preenchendo os defeitos causados pela corrosão deixando o perfil o mais próximo do original possível Remove corrosion on external surfaces, apply epoxy filling defects caused by corrosion, leaving the profile as close to the original as possible. |  |  |  |  |  |  |  |  | REPAROS MANUAIS |
|  | Realizar limpeza da peça conforme IAS-IP-0006 item 3.35 rev.3. Perform Cleaning iaw IAS-IP-0006 item 3.35 rev.3. |  |  |  |  |  |  |  |  | LIMPEZA QUÍMICA |
|  | Aplique a solução de dicromato no metal base exposto. Apply the dichromate solution to the bare metal. |  |  |  |  |  |  |  |  | LIMPEZA QUÍMICA |
|  | MASCARAMENTO: Isolar os prisioneiros, HELICOILS, faces de assentamento, PN e SN e locais onde não será aplicado coating. (task 70-32-11-300-801 – application of corrosion resistant paint) MASKING: Insolate studs, HELICOILS, seating faces, PN and SN and places where no coating will be applied. (task 70-32-11-300-801 - application of corrosion resistant paint). |  |  |  |  |  |  |  |  | PINTURA |
|  | Realizar pintura conforme IAS-IP-0005 Item 3.13 Rev.05 (task 70-32-11-300-801 – application of corrosion resistant paint). Apply coating per IAS-IP-0005 Item 3.13 Rev.05 (task 70-32-11-300-801 – application of corrosion resistant paint). |  |  |  |  |  |  |  |  | PINTURA |
|  | Proteger o componente lubrificando todas as gaiolas de localização dos rolamentos, prisioneiros e inserts. Protect the component by lubricating all bearing location cages, studs and inserts. |  |  |  |  |  |  |  |  | LIMPEZA QUÍMICA |
|  | Inspeção final Final inspection. |  |  |  |  |  |  |  |  | INSPEÇÃO |
| OBSERVAÇÕES (Observation): |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  |  | DATA (Date): |  |
| N/A |  |  |  | ANTONIO CLAUDIO |  |  |  |  | 27/02/2025 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)