| PN (PN): |  | SN: |  |  |  |  | Nº da OS (WO): |  |  |  | TLN: |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 23007217 |  | N/C |  |  |  |  | 041199 |  |  |  | 02127 |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  | ARTIGO/PARTE (Article/Part): |  |  |  |  |  | QUANT: |  |  |
| CAE-847564 |  |  | MOUNT ASSY |  |  |  |  |  | 01 |  |  |
| TSN: |  |  | CSN: |  |  | TSO: |  |  | CSO: |  |  |
| ITEM (Item) | DESCRIÇÃO DO SERVIÇO A EXECUTAR (Description of the work to be executed) |  |  | EXECUÇÃO (Execution) |  |  |  | *SETOR/FORNECEDOR (Sector/Supplier) |  |  |  |
|  | REMOVER O NÍQUEL POR PROCESSO QUIMICO. REMOVE NICKEL BY CHEMICAL PROCESS. |  |  |  |  |  |  | LIMPEZA QUIMICA |  |  |  |
|  | REALIZAR JATEAMENTO DE ESFERAS DE VIDRO CONFORME IAS-IP-0006 – 3,26, COM PRESSÃO MAXIMA DE 30 PSI. CARRY OUT BLASTING OF GLASS BEADS ACCORDING TO IAS-IP-0006 – 3.26, WITH MAXIMUM PRESSURE OF 30 PSI. |  |  |  |  |  |  | LIMPEZA ABRASIVA |  |  |  |
|  | REALIZAR SUAVIZAÇÃO DA CORROSÃO EXISTENTE NO FLANGE UTILIZANDO ESCOVA DE AÇO ROTATIVA. SOLVE THE EXISTING CORROSION ON THE FLANGE USING A ROTATING STEEL BRUSH. |  |  |  |  |  |  | LIMPEZA |  |  |  |
|  | REALIZAR APLICAÇÃO DE ELECTROLESS CONFORME PRPL 1-5, AMS2405 NA AREA TRATADA DO COMPONENTE. PERFORM ELECTROLESS APPLICATION IN ACCORDANCE WITH PRPL 1-5, AMS2405 ON THE TREATED AREA OF THE COMPONENT |  |  |  |  |  |  | GALVANOPLASTIA |  |  |  |
|  | REALIZAR INSPEÇÃO FINAL CONFORME OVERHAUL MANUAL PERFORM FINAL INSPECTION ACCORDING TO OVERHAUL MANUAL |  |  |  |  |  |  | INSPEÇÃO |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  |  | DATA (Date): |  |
|  |  |  |  |  | ANTONIO CLAUDIO |  |  |  |  | 28/02/2025 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)