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	Nº DO ARTIGO PRINCIPAL (Main Article):
	ARTIGO/PARTE (Article/Part):
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	ITEM
(Item)
	[bookmark: _Hlk184222911]TAREFA
(Task)
	[bookmark: _Hlk184222919]ETAPA
(Step)
	DESCRIÇÃO
(Description)

	1
	REPAIR SHOP	USINAGEM / MACHINING	USINAR A FACE DA BUCHA, DEIXANDO A ALTURA TOTAL= 1.421¨+ 0.001¨
ALTURA ATUAL É 1.424¨ 
VEJA A FIGURA ANEXA.

MACHINE THE BUSHING FACE, LEAVING THE TOTAL HEIGHT= 1.421 ̈ + 0.001 ̈ CURRENT HEIGHT IS 1.424 ̈ SEE THE ATTACHED FIGURE.

	2
	REPAIR SHOP	USINAGEM / MACHINING	USINAR A SUPERFÍCIE ¨B¨, DEIXANDO A PROFUNDIDADE= 0.9995¨ +OU- 0.001¨
ATUAL É 0.9978¨
VEJA A FIGURA ANEXA.

MACHINING THE SURFACE ̈B ̈, LEAVING DEPTH= 0.9995 ̈ +OR- 0.001 ̈ CURRENT IS 0.9978 ̈ SEE THE ATTACHED FIGURE.

	3
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	SUAVISAR OS CANTOS VIVOS DE AMBOS OS LADOS DA SUPERFÍCIE ¨A¨

SMOOTHING THE SHARP CORNERS ON BOTH SIDES OF THE SURFACE ̈A

	4
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	SUAVISAR AS DANIFICAÇÕES NA PAREDE E NOS CANTOS INTERNOS.

SMOOTH OUT DAMAGE TO THE WALL AND INSIDE CORNERS.

	5
	CHEMICAL CLEANING	LIMPAR / CLEAN	LIMPAR CONFORME A IP-0006, 3.10

CLEAR AS PER IP-0006, 3.10

	6
	NDT	END- PARTICULAS MAGNETICAS / NOT - MAGNETIC PARTICLE	EXECUTAR MPI: ASTM E 1444.
APRESENTOU INDICAÇÃO? (  )SIM      (  )NÃO

RUN MPI: ASTM E 1444. DID YOU PRESENT AN INDICATION? ( )YES ( )NO

	7
	CHEMICAL CLEANING	LIMPAR / CLEAN	LIMPAR CONFORME A IP-0006, 3.10

CLEAR AS PER IP-0006, 3.10

	8
	T56A	INSPEÇÃO / INSPECTION	INSPEÇÃO FINAL.

PROCURAR 1- EIXO PARA INSTALAR INTERNAMENTE.

FINAL INSPECTION. SEARCH 1- AXLE TO INSTALL INTERNALLY.
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· Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.
(In case of external service, the supplier must be indicated by the purchasing department)
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