| PN (PN): |  |  | SN: |  |  |  |  | Nº da OS (WO): |  |  | TLN: |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| AN310-5 |  |  | N/A |  |  |  |  | 040128 |  |  | 2686 |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  |  | ARTIGO/PARTE (Article/Part): |  |  | Serviço PrincipaL (Main Service) |  | QUANT: |  |  |
| 393291-21 |  |  |  | PARAFUSOS E PORCAS DIVERSOS MISCELLANEOUS BOLTS AND NUTS |  |  | REVISÃO GERAL / OVERHAUL |  | ITENS DIVERSOS MISCELLANEOUS ITEMS VIDE OBS. |  |  |
| TSN: IGN |  |  |  | CSN: N/A |  |  | TSO: N/A |  | CSO: N/A |  |  |
| ¦ITEM (Item) | TAREFA (Task) | ETAPA (Step) |  |  | DESCRIÇÃO (Description) |  |  |  |  |  |  |
| 1 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | EXECUTAR LIMPEZA CONFORME IP-0006, ITEM 3.35 PERFORM CLEANING IN ACCORDANCE WITH IP-0006, ITEM 3.35 |  |  |  |  |  |  |
| 2 | CHEMICAL CLEANING | DECAPAGEM / STRIPPING |  |  | EXECUTAR DECAPAGEM DOS ITEN CONFORME IAS IP-0006 ITEM 3.18 PERFORM STRIPPING OF ITENS IN ACCORDANCE WITH IAS IP-0006 ITEM 3.18 |  |  |  |  |  |  |
| 3 | CHEMICAL CLEANING | DEPOSIÇÃO DE NIQUEL-CADMIO / NICKEL-CADMIUM PLATING |  |  | APLICAR NOVO REVESTIMENTO DE NICKEL-CADMIUM (AMARELO) CONFORME SPOP 25 APPLY NEW NICKEL-CADMIUM COATING (YELLOW) ACCORDING TO SPOP 25 |  |  |  |  |  |  |
| 5 | CHEMICAL CLEANING | TRATAMENTO TERMICO / HEAT TREATMENT |  |  | EXECUTAR A CURA DOS BOLTS NO FORNO NA TEMPERATURA DE 180°C A 210°C PELO TEMPO DE 3 HORAS. CURE THE BOLTS IN THE OVEN AT A TEMPERATURE OF 180°C TO 210°C FOR 3 HOURS. |  |  |  |  |  |  |
| 6 | T56A | INSPEÇÃO / INSPECTION |  |  | REALIZAR INSPEÇÃO FINAL PERFORM FINAL INSPECTION |  |  |  |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  | DATA (Date): |  |
| Manter os itens separados conforme apresentado na entrega. ATENÇÃO: Parafusos, porcas e suportes |  |  |  |  |  | Leonardo dos Santos Gomes |  |  |  | 12/03/2025 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)