| PN (PN): |  |  | SN: |  |  |  |  | Nº da OS (WO): |  |  | TLN: |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| RR30000246 |  |  | GK30457 |  |  |  |  | 044641 |  |  | 02027 |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  |  | ARTIGO/PARTE (Article/Part): |  |  | Serviço PrincipaL (Main Service) |  | QUANT: |  |  |
| RR300 / RRE-200280 |  |  |  | Spline Adapter |  |  | REPARO / REPAIR |  | 01 EA |  |  |
| TSN: |  |  |  | CSN: |  |  | TSO: |  | CSO: |  |  |
| ITEM (Item) | TAREFA (Task) | ETAPA (Step) |  |  | DESCRIÇÃO (Description) |  |  |  |  |  |  |
| 1 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | Remova quimicamente a prata pré-existente e o níquel subjacente no spline adapter (Ref. AMS 2403) Chemically strip the pre-existing silver and underlying nickel on the 2nd-stage turbine splined adapter (Ref. AMS 2403). |  |  |  |  |  |  |
| 2 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | Restaure banho de prata nas estrias externas com uma espessura de 0.0001-0.0003 pol. (0,003-0,008 mm) (Ref. AMS 2410 ou AMS 2412). Restore the silver plate to the external splines to a thickness of 0.0001-0.0003 in. (0.003-0.008 mm) (Ref. AMS 2410 or AMS 2412). |  |  |  |  |  |  |
| 3 | ACESSÓRIOS | TESTE /TEST |  |  | Dentro de quatro horas após o banho, faça o alívio da fragilização por hidrogênio aquecido a 350-550°F (177-288°C) durante duas horas (Ref. AMS 2410 ou AMS 2412). Within four hours after you plate, do the hydrogen enbrittlement relief heated to 350-550°F (177-288°C) for two hours (Ref. AMS 2410 or AMS 2412). |  |  |  |  |  |  |
|  | RR300 | INSPEÇÃO / INSPECTION |  |  | Inspeção final Final inspection. |  |  |  |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  | DATA (Date): |  |
|  |  |  |  |  |  | Patrick Dimas |  |  |  | 23/06/2025 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)