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	PN (PN):
	SN:
	Nº da OS (WO):
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	Nº DO ARTIGO PRINCIPAL (Main Article):
	ARTIGO/PARTE (Article/Part):
	Serviço PrincipaL
(Main Service)
	QUANT:

	RR300 / RRE-200280
	Spline Adapter
	REPARO / REPAIR	01 EA

	TSN:
	CSN:
	TSO:
	CSO:

	ITEM
(Item)
	[bookmark: _Hlk184222911]TAREFA
(Task)
	[bookmark: _Hlk184222919]ETAPA
(Step)
	DESCRIÇÃO
(Description)

	1
	CHEMICAL CLEANING	LIMPAR / CLEAN	Remova quimicamente a prata pré-existente e o níquel subjacente no spline adapter (Ref. AMS 2403)

Chemically strip the pre-existing silver and underlying nickel on the 2nd-stage turbine splined adapter (Ref. AMS 2403).

	2
	CHEMICAL CLEANING	LIMPAR / CLEAN	Restaure banho de prata nas estrias externas com uma espessura de 0.0001-0.0003 pol. (0,003-0,008 mm) (Ref. AMS 2410 ou AMS 2412). 

Restore the silver plate to the external splines to a thickness of 0.0001-0.0003 in. (0.003-0.008 mm) (Ref. AMS 2410 or AMS 2412).

	3
	ACESSÓRIOS	TESTE /TEST	Dentro de quatro horas após o banho, faça o alívio da fragilização por hidrogênio aquecido a 350-550°F (177-288°C) durante duas horas (Ref. AMS 2410 ou AMS 2412).

Within four hours after you plate, do the hydrogen enbrittlement relief heated to 350-550°F (177-288°C) for two hours (Ref. AMS 2410 or AMS 2412).

	
	RR300	INSPEÇÃO / INSPECTION	Inspeção final

Final inspection.

	OBSERVAÇÕES
(Observation):
	ASSINATURA DO SOLICITANTE 
(Signature):
	DATA 
(Date):

	[bookmark: Texto2]     
	Patrick Dimas
	23/06/2025


· Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.
(In case of external service, the supplier must be indicated by the purchasing department)
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