| PN (PN): |  |  | SN: |  |  |  |  | Nº da OS (WO): |  |  | TLN:02188 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 6844756 |  |  | 13606 |  |  |  |  | IAS |  |  |  |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  |  | ARTIGO/PARTE (Article/Part): |  |  | Serviço PrincipaL (Main Service) |  | QUANT: |  |  |
| AE- 108598 |  |  |  | COUPLING ADAPTER |  |  | REVISÃO GERAL / OVERHAUL |  | 1 |  |  |
| ITEM (Item) | TAREFA (Task) | ETAPA (Step) |  |  | DESCRIÇÃO (Description) |  |  |  |  |  |  |
| 1 | NDT | END- PARTICULAS MAGNETICAS / NOT - MAGNETIC PARTICLE |  |  | EXECUTAR MPI: ASTM E 1444. APRESENTOU INDICAÇÃO? ( )SIM ( )NÃO RUN MPI: ASTM E 1444. DID YOU PRESENT AN INDICATION? ( )YES ( )NO |  |  |  |  |  |  |
| 2 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 3 | REPAIR SHOP | JATEAR / BLAST |  |  | ISOLAR E JATEAR OS DENTES, COM ÓXIDO DE ALUMÍNIO, GRÃO 220 ou 240 INSULATE AND BLAST TEETH WITH ALUMINUM OXIDE, GRIT 220 or 240 |  |  |  |  |  |  |
| 4 | REPAIR SHOP | PINTURA / PAINTING |  |  | APLICAR NOS DENTES ALSEAL 370. APPLY TO ALSEAL 370 TEETH. |  |  |  |  |  |  |
| 5 | REPAIR SHOP | TRATAMENTO TERMICO / HEAT TREATMENT |  |  | REMOVER AS ISOLAÇÕES E AQUECER EM FORNO POR 1- HORA A 185° C. REMOVE THE INSULATIONS AND HEAT IN THE OVEN FOR 1-HOUR AT 185° C. |  |  |  |  |  |  |
| 6 | T56A | INSPEÇÃO / INSPECTION |  |  | INSPEÇÃO FINAL. ( )APROVADO ( )REPROVADO FINAL INSPECTION. ( )APPROVED ( )FAILED |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  | DATA 01/08/2025 (Date): |  |
|  |  |  |  |  |  | VILSON BARBOSA |  |  |  | 01/08/2025 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)