| PN (PN): |  |  | SN: |  |  |  |  | Nº da OS (WO): |  |  | TLN: |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 23071313 |  |  | UF22002 |  |  |  |  | 046420 |  |  | 02127 |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  |  | ARTIGO/PARTE (Article/Part): |  |  | Serviço PrincipaL (Main Service) |  | QUANT: |  |  |
| M250-C30P / CAT-97878 |  |  |  | Inner Shaft |  |  | PINTURA / PAINTING |  | 01 EA |  |  |
| TSN: |  |  |  | CSN: |  |  | TSO: |  | CSO: |  |  |
| ITEM (Item) | TAREFA (Task) | ETAPA (Step) |  |  | DESCRIÇÃO (Description) |  |  |  |  |  |  |
|  | CHEMICAL CLEANING | DEPOSIÇÃO DE NIQUEL / NICKEL PLATING |  |  | Aplicar electroless nickel plating 0.0005-0.0007 inches conforme AMS 2405, nas areas indicadas na Figura 317 (SHEET 2 DE 3) – 72-50-00 page 338. Apply electroless nickel plating 0.0005-0.0007 inches according to AMS 2405, in the areas indicated in Figure 317 (SHEET 2 OF 3) – 72-50-00 page 338 |  |  |  |  |  |  |
|  | CHEMICAL CLEANING | TRATAMENTO TERMICO / HEAT TREATMENT |  |  | Tratamento térmico: - temperatura de 350° F +/- 15° F (177° C +/- 8° C) - tempo – 3 horas - NCC forno: _____________ val.: _____________ Heat treatment: - temperature of 350° F +/- 15° F (177° C +/- 8° C) - tempo – 3 hours |  |  |  |  |  |  |
|  | M250 | INSPEÇÃO / INSPECTION |  |  | REALIZAR INSPEÇÃO DO NÍQUEL APLIDADO. PERFORM INSPECTION OF APPLIED NICKEL |  |  |  |  |  |  |
| 1 | REPAIR SHOP | PINTURA / PAINTING |  |  | Aplicar Alseal 518 / 598 conforme procedimento IAS-IP-0005 Item 3.27 Rev.05. Ref. Fig. 324 sheet 1 em anexo. (REPAIR-14 TASK 70-32-15-300-814). Nota2: Não deve haver bolhas, pingos, rachaduras e a superfície deve ser lisa. Apply Alseal 518 / 598 per IAS-IP-0005 Item 3.27 Rev.05. Ref. Fig. 324 sheet 1 attached. (REPAIR-14 TASK 70-32-15-300-814). Note: There must be no blisters, drips, mud cracks, or beading and the surface must be smooth. |  |  |  |  |  |  |
| 2 | M250 | INSPEÇÃO / INSPECTION |  |  | Inspeção final (Realizar preservação do artigo protegendo contra danos de impacto e corrosão). Final inspection (Preserve the part and protect to prevent any damages and corrosion). |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  | DATA (Date): |  |
|  |  |  |  |  |  | ANTONIO CLAUDIO |  |  |  | 08/08/2025 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)