| PN (PN): |  |  | SN: |  |  |  |  | Nº da OS (WO): |  |  | TLN:02188 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 6846907 |  |  | BL-8436 |  |  |  |  | IAS |  |  |  |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  |  | ARTIGO/PARTE (Article/Part): |  |  | Serviço PrincipaL (Main Service) |  | QUANT: |  |  |
| AE- 109008 |  |  |  | COUPLING SHAFT |  |  | REVISÃO GERAL / OVERHAUL |  | 1 |  |  |
| ITEM (Item) | TAREFA (Task) | ETAPA (Step) |  |  | DESCRIÇÃO (Description) |  |  |  |  |  |  |
| 1 | REPAIR SHOP | USINAGEM / MACHINING |  |  | RETIFICAR O DIÂMETRO ESFÉRICO, DEIXANDO= 1.530¨ +ou- 0.002¨ RECTIFY THE SPHERICAL DIAMETER, LEAVING= 1.530 ̈ +or- 0.002 |  |  |  |  |  |  |
| 2 | CHEMICAL CLEANING | TRATAMENTO TERMICO / HEAT TREATMENT |  |  | TRATAMENTO TÉRMICO EM 135° C POR 5- HORAS. HEAT TREATMENT AT 135° C FOR 5-HOURS. |  |  |  |  |  |  |
| 3 | NDT | END- PARTICULAS MAGNETICAS / NOT - MAGNETIC PARTICLE |  |  | EXECUTAR MPI: ASTM E 1444. APRESENTOU INDICAÇÃO? ( )SIM ( )NÃO RUN MPI: ASTM E 1444. DID YOU PRESENT AN INDICATION? ( )YES ( )NO |  |  |  |  |  |  |
| 4 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 5 | CHEMICAL CLEANING | DEPOSIÇÃO DE CROMO / CHROME PLATING |  |  | ISOLAR E APLICAR CROMO DURO (AMS 2406) NO DIÂMETRO ESFÉRICO, QUE NO FINAL FICARÁ= 1.5365¨ ISOLATE AND APPLY HARD CHROME (AMS 2406) TO THE SPHERICAL DIAMETER, WHICH IN THE END WILL BE = 1.5365 |  |  |  |  |  |  |
| 6 | CHEMICAL CLEANING | TRATAMENTO TERMICO / HEAT TREATMENT |  |  | TRATAMENTO TÉRMICO EM 135° C POR 8- HORAS. HEAT TREATMENT AT 135° C FOR 8-HOURS. |  |  |  |  |  |  |
| 7 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 8 | NDT | END- LIQUIDO PENETRANTE / NDT - FLUORESCENT PENETRANT INSPECTION |  |  | EXECUTAR MPI: ASTM E 1444. APRESENTOU INDICAÇÃO? ( )SIM ( )NÃO RUN MPI: ASTM E 1444. DID YOU PRESENT AN INDICATION? ( )YES ( )NO |  |  |  |  |  |  |
| 9 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 10 | NDT | END- LIQUIDO PENETRANTE / NDT - FLUORESCENT PENETRANT INSPECTION |  |  | EXECUTAR FPI: ASTM E 1417, METHOD-A, LEVEL-3. APRESENTOU INDICAÇÃO? ( )SIM ( )NÃO RUN FPI: ASTM E 1417, METHOD-A, LEVEL-3. DID YOU PRESENT AN INDICATION? ( )YES ( )NO |  |  |  |  |  |  |
| 11 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 12 | CHEMICAL CLEANING | JATEAR / BLAST |  |  | ISOLAR E APLICAR GLASS BEAD NAS ESTRIAS, COM BAIXA PRESSÃO. ISOLATE AND APPLY GLASS BEAD TO STRETCH MARKS, WITH LOW PRESSURE. ISOLATE AND APPLY GLASS BEAD TO STRETCH MARKS, WITH LOW PRESSURE. |  |  |  |  |  |  |
| 13 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 14 | NDT | END- PARTICULAS MAGNETICAS / NOT - MAGNETIC PARTICLE |  |  | EXECUTAR MPI: ASTM E 1444. APRESENTOU INDICAÇÃO? ( )SIM ( )NÃO RUN MPI: ASTM E 1444. DID YOU PRESENT AN INDICATION? ( )YES ( )NO |  |  |  |  |  |  |
| 15 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 16 | REPAIR SHOP | PINTURA / PAINTING |  |  | APLICAR SOMENTE ¨UMA¨ FINA CAMADA DE ALSEAL 370 NAS ESTRIAS. APPLY ONLY A THIN LAYER OF ALSEAL 370 ON THE STRETCH MARKS. |  |  |  |  |  |  |
| 17 | REPAIR SHOP | BALANCEAMENTO / BALANCING |  |  | EXECUTAR BALANCEAMENTO. PERFORM BALANCING. |  |  |  |  |  |  |
| 18 | T56A | INSPEÇÃO / INSPECTION |  |  | INSPEÇÃO FINAL. ( )APROVADO ( )REPROVADO FINAL INSPECTION. ( )APPROVED ( )FAILED |  |  |  |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  | DATA 08/08/2025 (Date): |  |
|  |  |  |  |  |  | VILSON BARBOSA |  |  |  | 08/08/2025 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)