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	DESCRIÇÃO
(Description)

	1
	REPAIR SHOP	USINAGEM / MACHINING	RETIFICAR O DIÂMETRO ESFÉRICO, DEIXANDO= 1.530¨ +ou- 0.002¨

RECTIFY THE SPHERICAL DIAMETER, LEAVING= 1.530 ̈ +or- 0.002

	2
	CHEMICAL CLEANING	TRATAMENTO TERMICO / HEAT TREATMENT	TRATAMENTO TÉRMICO EM 135° C POR 5- HORAS.

HEAT TREATMENT AT 135° C FOR 5-HOURS.

	3
	NDT	END- PARTICULAS MAGNETICAS / NOT - MAGNETIC PARTICLE	EXECUTAR MPI: ASTM E 1444.
APRESENTOU INDICAÇÃO? (  )SIM     (  )NÃO

RUN MPI: ASTM E 1444. DID YOU PRESENT AN INDICATION? ( )YES ( )NO

	4
	CHEMICAL CLEANING	LIMPAR / CLEAN	LIMPAR CONFORME A IP-0006, 3.10

CLEAR AS PER IP-0006, 3.10

	5
	CHEMICAL CLEANING	DEPOSIÇÃO DE CROMO / CHROME PLATING	ISOLAR E APLICAR CROMO DURO (AMS 2406) NO DIÂMETRO ESFÉRICO, QUE NO FINAL FICARÁ= 1.5365¨

ISOLATE AND APPLY HARD CHROME (AMS 2406) TO THE SPHERICAL DIAMETER, WHICH IN THE END WILL BE = 1.5365

	6
	CHEMICAL CLEANING	TRATAMENTO TERMICO / HEAT TREATMENT	TRATAMENTO TÉRMICO EM 135° C POR 8- HORAS.

HEAT TREATMENT AT 135° C FOR 8-HOURS.

	7
	CHEMICAL CLEANING	LIMPAR / CLEAN	LIMPAR CONFORME A IP-0006, 3.10

CLEAR AS PER IP-0006, 3.10

	8
	NDT	END- LIQUIDO PENETRANTE / NDT - FLUORESCENT PENETRANT INSPECTION	EXECUTAR MPI: ASTM E 1444.
APRESENTOU INDICAÇÃO? (  )SIM    (  )NÃO

RUN MPI: ASTM E 1444. DID YOU PRESENT AN INDICATION? ( )YES ( )NO

	9
	CHEMICAL CLEANING	LIMPAR / CLEAN	LIMPAR CONFORME A IP-0006, 3.10

CLEAR AS PER IP-0006, 3.10

	10
	NDT	END- LIQUIDO PENETRANTE / NDT - FLUORESCENT PENETRANT INSPECTION	EXECUTAR FPI: ASTM E 1417, METHOD-A, LEVEL-3.
APRESENTOU INDICAÇÃO? (  )SIM    (  )NÃO

RUN FPI: ASTM E 1417, METHOD-A, LEVEL-3. DID YOU PRESENT AN INDICATION? ( )YES ( )NO

	11
	CHEMICAL CLEANING	LIMPAR / CLEAN	LIMPAR CONFORME A IP-0006, 3.10

CLEAR AS PER IP-0006, 3.10

	12
	CHEMICAL CLEANING	JATEAR / BLAST	ISOLAR E APLICAR GLASS BEAD NAS ESTRIAS, COM BAIXA PRESSÃO.
ISOLATE AND APPLY GLASS BEAD TO STRETCH MARKS, WITH LOW PRESSURE.
ISOLATE AND APPLY GLASS BEAD TO STRETCH MARKS, WITH LOW PRESSURE.

	13
	CHEMICAL CLEANING	LIMPAR / CLEAN	LIMPAR CONFORME A IP-0006, 3.10

CLEAR AS PER IP-0006, 3.10

	14
	NDT	END- PARTICULAS MAGNETICAS / NOT - MAGNETIC PARTICLE	EXECUTAR MPI: ASTM E 1444.
APRESENTOU INDICAÇÃO? (  )SIM     (  )NÃO

RUN MPI: ASTM E 1444. DID YOU PRESENT AN INDICATION? ( )YES ( )NO

	15
	CHEMICAL CLEANING	LIMPAR / CLEAN	
LIMPAR CONFORME A IP-0006, 3.10

CLEAR AS PER IP-0006, 3.10

	16
	REPAIR SHOP	PINTURA / PAINTING	APLICAR SOMENTE ¨UMA¨ FINA CAMADA DE ALSEAL 370 NAS ESTRIAS.

APPLY ONLY A THIN LAYER OF ALSEAL 370 ON THE STRETCH MARKS.

	17
	REPAIR SHOP	BALANCEAMENTO / BALANCING	EXECUTAR BALANCEAMENTO.

PERFORM BALANCING.

	18
	T56A	INSPEÇÃO / INSPECTION	INSPEÇÃO FINAL.
(  )APROVADO        (  )REPROVADO

FINAL INSPECTION. ( )APPROVED ( )FAILED
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	DATA 08/08/2025
(Date):

	[bookmark: Texto2]     
	VILSON BARBOSA
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· Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.
(In case of external service, the supplier must be indicated by the purchasing department)
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