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	REGISTRO
	REVISÃO
	04

	
	RECORD
	REVISION
	

	CODIGO | CODE
	SOLICITAÇÃO DE SERVIÇOS COMPLEMENTARES
	PÁGINA
	1/1

	IAS-RG-0103
	SUPPLEMENTARY REQUEST
	PAGE
	



	PN (PN):
	SN:
	Nº da OS (WO):
	TLN:02188

	6842656
	XX8821
	IAS
	

	Nº DO ARTIGO PRINCIPAL (Main Article):
	ARTIGO/PARTE (Article/Part):
	Serviço PrincipaL
(Main Service)
	QUANT:

	IAS   /   AE-109024
	AIR INLET HOUSING
	REVISÃO GERAL / OVERHAUL	1

	
	
	
	

	ITEM
(Item)
	[bookmark: _Hlk184222911]TAREFA
(Task)
	[bookmark: _Hlk184222919]ETAPA
(Step)
	DESCRIÇÃO
(Description)

	1
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	MONTAR O CAGE E FRENAR COM 2- PINOS P/N= MS9105-53

MOUNTING THE CAGE AND BRAKING WITH 2-PIN P/N= MS9105-53

	2
	REPAIR SHOP	RETIFICA / RECTIFY	RETIFICAR O DIÂMETRO INTERNO DO CAGE CROMADO, DEIXANDO= 4.3340¨+ou-0.0002¨
CENTRAR PELO DIÂMETRO EXTERNO DA FACE ADJACENTE.
REMOVER CANTO VIVO.

RECTIFY THE INNER DIAMETER OF THE CHROME CAGE, ALLOWING= 4.3340 ̈+or-0.0002 ̈ CENTER BY THE OUTSIDE DIAMETER OF THE ADJACENT FACE. REMOVE LIVE CORNER.

	3
	CHEMICAL CLEANING	LIMPAR / CLEAN	EXECUTAR LIMPEZA CONFORME A IP-0006, 3.10

PERFORM CLEANING IN ACCORDANCE WITH IP-0006, 3.10

	4
	NDT	END- LIQUIDO PENETRANTE / NDT - FLUORESCENT PENETRANT INSPECTION	EXECUTAR FPI: ASTM E 1417, METHOD-A, LEVEL 3.
APRESENTOU INDICAÇÃO? (  )SIM       (  )NÃO

RUN FPI: ASTM E 1417, METHOD-A, LEVEL 3. DID YOU PRESENT AN INDICATION? ( )YES ( )NO

	5
	CHEMICAL CLEANING	LIMPAR / CLEAN	LIMPAR CONFORME A IP-0006, 3.10

CLEAR AS PER IP-0006, 3.10

	6
	REPAIR SHOP	ISOLAÇÃO / MASK	ISOLAR OS PRISIONEIROS, INSERTS E ÁREAS DE CONTATO.

ISOLATE STUDS, INSERTS AND CONTACT AREAS.

	7
	REPAIR SHOP	PINTURA / PAINTING	PINTAR COM: PRIMER PA-0060  E  CINZA PA-0065.

PAINT WITH: PRIMER PA-0060 AND GRAY PA-0065.

	8
	REPAIR SHOP	REMOVER ISOLAMENTO / REMOVE MASK	REMOVER AS ISOLAÇÕES E OS EXCESSOS DE TINTA.

REMOVE INSULATION AND EXCESS PAINT.

	9
	REPAIR SHOP	PINTURA / PAINTING	ISOLAR E APLICAR EMBORRACHAMENTO NO BORDO DE ATAQUE DOS STRUTS.

ISOLATE AND APPLY RUBBER COATING TO THE LEADING EDGE OF THE STRUTS.

	10
	T56A	INSPEÇÃO / INSPECTION	INSPEÇÃO FINAL. Lubrificar os prisioneiros.
(  )APROVADO      (  )REPROVADO

FINAL INSPECTION. ( )APPROVED ( )FAILED
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· Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.
(In case of external service, the supplier must be indicated by the purchasing department)
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