| PN (PN): |  |  | SN: |  |  |  |  | Nº da OS (WO): |  |  | TLN: |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 6871447 |  |  | 5125 |  |  |  |  | PRINCIPAL |  |  | 02188 |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  |  | ARTIGO/PARTE (Article/Part): |  |  | Serviço PrincipaL (Main Service) |  | QUANT: |  |  |
| AE-109692 |  |  |  | COMPRESSOR CASING |  |  | REVISÃO GERAL / OVERHAUL |  | 01 |  |  |
| TSN: |  |  |  | CSN: |  |  | TSO: |  | CSO: |  |  |
| ITEM (Item) | TAREFA (Task) | ETAPA (Step) |  |  | DESCRIÇÃO (Description) |  |  |  |  |  |  |
| 1 | REPAIR SHOP | USINAGEM / MACHINING |  |  | USINAR O DIAMETRO INTERNO “P”, DEIXANDO COM 15.139” +- 0.001. NOTA: CENTRAR PELO DIÂMETRO INTERNO QUE ALOJA A VANE DO 14° ESTÁGIO, DEIXAR MANCHAS. |  |  |  |  |  |  |
| 2 | REPAIR SHOP | USINAGEM / MACHINING |  |  | USINAR OS DIÂMETROS INTERNOS DOS 14 ESTÁGIOS, ATÉ REMOVER O MATERIAL BÁSICO E DAR RÚSTICO. MACHINING THE INTERNAL DIAMETERS OF THE 14 STAGES, UNTIL THE BASIC MATERIAL IS REMOVED AND ROUGHENED. |  |  |  |  |  |  |
| 3 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | EXECUTAR LIMPEZA CONF. IP-006, 3.10 PERFORM CLEANING CONF. IP-006, 3.10 |  |  |  |  |  |  |
| 4 | CHEMICAL CLEANING | NON-DESTRUCTIVE TESTING |  |  | EXECUTAR FPI: ASTM E 1417, METODO-A, LEVEL-2. APRESENTOU INDICAÇÃO? ( )SIM ( )NÃO. PERFORM FPI: ASTM E 1417, METHOD-A, LEVEL-2. HAS IT BEEN INDICATED? ( )YES ( )NO. |  |  |  |  |  |  |
| 5 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | EXECUTAR LIMPEZA CONF. IP-006, 3.10 PERFORM CLEANING CONF. IP-006, 3.10 |  |  |  |  |  |  |
| 6 | REPAIR SHOP | ISOLAÇÃO / MASK |  |  | ISOLAR AS ROSCAS, FUROS E AREAS DE CONTATO. INSULATE THREADS, HOLES AND CONTACT AREAS. |  |  |  |  |  |  |
| 7 | REPAIR SHOP | PINTURA / PAINTING |  |  | APLICAR EXTERNAMENTE, SERMETEL W OU ALSEAL 518, CONF. IP-006, 3.17. APPLY SERMETEL W OR ALSEAL 518 EXTERNALLY, CONF. IP-006, 3.17 |  |  |  |  |  |  |
| 8 | REPAIR SHOP | REMOVER ISOLAMENTO / REMOVE MASK |  |  | REMOVER AS ISOLAÇÕES E EXCESSOS. REMOVE INSULATION AND EXCESS |  |  |  |  |  |  |
| 9 | REPAIR SHOP | METALIZAÇÃO / THERMAL SPRAY |  |  | ISOLAR E METALIZAR INTERNAMENTE COM METCO 405 E APÓS COMPLETAR COM ALUMÍNIO METCO SF(1030508). INSULATE AND METALLIZE INTERNALLY WITH METCO 405 AND THEN COMPLETE WITH ALUMINIUM METCO SF(1030508) |  |  |  |  |  |  |
| 10 | REPAIR SHOP | USINAGEM / MACHINING |  |  | USINAR O ALUMÍNIO INTERNO, LIMPANDO AS CANALETAS CONF. A FIGURA DA PÁGINA 924, ANEXA. MACHINE THE INTERNAL ALUMINUM, CLEANING THE GROOVES ACCORDING TO THE FIGURE ON PAGE 924, ATTACHED. THE FIGURE ON PAGE 924, ATTACHED. |  |  |  |  |  |  |
| 11 | REPAIR SHOP | USINAGEM / MACHINING |  |  | USINAR OS 14 DIAMETROS INTERNOS COM ALUMINIO DEIXANDO: DO 1 AO 9 ESTÁGIO: 14._______” DO 10 AO 14 ESTAGIO: 14._______” CENTRADO PELOS DIAMETRO “Q” E “P” CONF. A FIGURA DA PAG. 804 ANEXA. MACHINING THE 14 INTERNAL DIAMETERS FROM ALUMINUM, LEAVING: FROM STAGE 1 TO 9: 14._______” FROM STAGE 10 TO 14: 14._______” CENTERED ON THE DIAMETERS "Q" AND "P" ACCORDING TO FIGURE ON PAGE 804 ATTACHED. |  |  |  |  |  |  |
| 12 | REPAIR SHOP | USINAGEM / MACHINING |  |  | USINAR OS CHANFROS, CONF. A FIGURA DA PAGINA 804, ANEXA. MACHINING THE CHAMFERS, ACCORDING TO THE FIGURE ON PAGE 804, ATTACHED |  |  |  |  |  |  |
| 13 | REPAIR SHOP | USINAGEM / MACHINING |  |  | PREPARAR AS AREAS USINADAS, REMOVENDO OS EXCESSOS E POLINDO AS ROSCAS, DIAMETROS E FACES DE CONTATO. PREPARING THE MACHINED AREAS, REMOVING EXCESS AND POLISHING THE THREADS, DIAMETERS AND CONTACT FACES. |  |  |  |  |  |  |
| 14 | T56A | MONTAG EM/ ASSEMBLY |  |  | MONTAR AS VANES E CALIBRAR AS ALTURAS CONF. A FIGURA DA PÁGINA 405 ANEXA. ASSEMBLE THE VANS AND CALIBRATE THE HEIGHTS ACCORDING TO THE FIGURE ON PAGE 405 ATTACHED |  |  |  |  |  |  |
| 15 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | REMOVER OS EXCESSOS DAS PONTAS DOS ARCOS DAS VANES, DEIXANDO ABAIXO DAS FACES DO CARTER. REMOVE THE EXCESS FROM THE ENDS OF THE VANES' ARCHES, LEAVING THEM BELOW THE CRANKCASE FACES |  |  |  |  |  |  |
| 16 | REPAIR SHOP | USINAGEM / MACHINING |  |  | USINAR O DIAMETRO INTERNO DOS SEALS DAS VANES, CONF. A TABELA DA PÁGINA 405 ANEXA. MACHINE THE INSIDE DIAMETER OF THE VANES' SEALS, ACCORDING TO THE TABLE ON PAGE 40 ATTACHED. THE TABLE ON PAGE 405 ATTACHED. |  |  |  |  |  |  |
| 17 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | EXECUTAR LIMPEZA CONF. IP-006, 3.09. CARRY OUT CLEANING IN ACCORDANCE WITH IP-006, 3.09. |  |  |  |  |  |  |
| 18 | T56A | INSPEÇÃO / INSPECTION |  |  | INSPEÇÃO FINAL. ( )APROVADO ( )REPROVADO FINAL INSPECTION. ( ) APPROVED ( )REPROVED |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  | DATA (Date): |  |
|  |  |  |  |  |  | AUGUSTO ROSA |  |  |  | 22/08/2025 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)