| PN (PN): |  |  | SN: |  |  |  |  | Nº da OS (WO): |  |  | TLN: |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 6875121 |  |  | TSO049A |  |  |  |  | 44996 |  |  | 2188 |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  |  | ARTIGO/PARTE (Article/Part): |  |  | Serviço PrincipaL (Main Service) |  | QUANT: |  |  |
| --- |  |  |  | LEVER, FUEL CUTOFF OUTPUT |  |  | REPARO / REPAIR |  | 4 |  |  |
| TSN: |  |  |  | CSN: |  |  | TSO: |  | CSO: |  |  |
| ITEM (Item) | TAREFA (Task) | ETAPA (Step) |  |  | DESCRIÇÃO (Description) |  |  |  |  |  |  |
| 02 | CHEMICAL PROCESS | LIMPEZA |  |  | Realize a decapagem do componente em acordo a IAS-IT-0273 Perform component stripping in accordance with IAS-IT-0273. |  |  |  |  |  |  |
| 03 | CHEMICAL PROCESS | APLICAÇÃO |  |  | Realize a aplicação do revestimento do componente em acordo a TASK 70-01-11-300-801 (Cadmium Touch-up Plating Maintenance Practices) do manual de TLN 02188, página 75. Apply the component coating in accordance with TASK 70-01-11-300-801 (Cadmium Touch-up Plating Maintenance Practices) in the TLN 02188 manual, page 75. OBS: APLICAR BANHO DE CÁDMIO COM CROMATO NOTE: APPLY CADMIUM PLATING WITH CHROMATE |  |  |  |  |  |  |
| 04 | ACESSÓRIOS | INSPEÇÃO |  |  | Realizar inspeção do componente a fim de garantir que a aplicação do “coating” está adequada. Inspect the component to ensure that the coating has been applied properly. |  |  |  |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  | DATA (Date): |  |
| Juntamente do LEVER, acompanha para serviço os seguintes itens: Along with the LEVER, the following items are included for service: Lever, Condition – PN 6812634 Pointer, Coordinator – PN 6812620 Cap, Coordinator – PN 6812619 Lever, Coordinator, Prop Setting – PN 6814486 |  |  |  |  |  | Arthur Castro |  |  |  | 25/08/25 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)