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	Nº DO ARTIGO PRINCIPAL (Main Article):
	ARTIGO/PARTE (Article/Part):
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	ITEM
(Item)
	[bookmark: _Hlk184222911]TAREFA
(Task)
	[bookmark: _Hlk184222919]ETAPA
(Step)
	DESCRIÇÃO
(Description)

	1
	REPAIR SHOP	USINAGEM / MACHINING	USINAR AS LATERAIS INTERNAS DO RASGO, DEIXANDO= 0.126¨+ou- 0.002¨

MACHINE THE INNER SIDES OF THE SLOT, LEAVING= 0.126 ̈+or- 0.002

	7
	REPAIR SHOP	METALIZAÇÃO / THERMAL SPRAY	ISOLAR E METALIZAR A CANALETA COM METCO 450 ou METCO 68F-NS-1

INSULATING AND METALLIZING CHANNEL WITH METCO 450 or METCO 68F-NS-1

	8
	REPAIR SHOP	RETIFICA / RECTIFY	RETIFICAR AS FACES INTERNAS DA CANALETA METALIZADA, DEIXANDO A LARGURA INTERNA = 0.104¨+ou- 0.001¨
REMOVER CANTOS VIVOS. CENTRAR PELO ¨B¨ ou ¨E¨
VEJA A FIGURA ANEXA.

RECTIFY THE INTERNAL FACES OF THE METALLIZED GUTTER, LEAVING THE INTERNAL WIDTH = 0.104 ̈+or- 0.001 ̈ REMOVE SHARP CORNERS. CENTER BY ̈B ̈ or ̈E ̈ SEE THE ATTACHED FIGURE.

	9
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	PREPARAR ÁREAS USINADAS, REMOVENDO OS EXCESSOS.

PREPARE MACHINED AREAS, REMOVING EXCESSES.

	10
	CHEMICAL CLEANING	LIMPAR / CLEAN	LIMPAR CONFORME A IP-0006, 3.10

CLEAR AS PER IP-0006, 3.10

	11
	NDT	END- LIQUIDO PENETRANTE / NDT - FLUORESCENT PENETRANT INSPECTION	EXECUTAR FPI: ASTM E 1417, METHOD-A, LEVEL-3.
APRESENTOU INDICAÇÃO? (  )SIM    (  )NÃO

RUN FPI: ASTM E 1417, METHOD-A, LEVEL-3. DID YOU PRESENT AN INDICATION? ( )YES ( )NO

	12
	CHEMICAL CLEANING	LIMPAR / CLEAN	LIMPAR CONFORME A IP-0006, 3.10

CLEAR AS PER IP-0006, 3.10

	13
	T56A	INSPEÇÃO / INSPECTION	INSPEÇÃO FINAL.
(  )APROVADO     (  )REPROVADO

FINAL INSPECTION. ( )APPROVED ( )FAILED
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· Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.
(In case of external service, the supplier must be indicated by the purchasing department)
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