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	DESCRIÇÃO
(Description)

	1
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	DESOVALIZAR (0.170¨) A ÁREA CENTRAL DO CORPO NA PRENSA, ENTRE 2- PEDAÇOS DE MADEIRA.

DESOVALIZE (0.170 ̈) THE CENTRAL AREA OF THE BODY IN THE PRESS, BETWEEN 2- PIECES OF WOOD.

	2
	NDT	END- LIQUIDO PENETRANTE / NDT - FLUORESCENT PENETRANT INSPECTION	EXECUTAR FPI: ASTM E 1417, METHOD-A, LEVEL-3
APRESENTOU INDICAÇÃO? (  )SIM      (  )NÃO

RUN FPI: ASTM E 1417, METHOD-A, LEVEL-3 DID YOU PRESENT AN INDICATION? ( )YES ( )NO

	3
	CHEMICAL CLEANING	LIMPAR / CLEAN	LIMPAR CONFORME A IP-0006, 3.10
NÃO DESMARCAR AS TRINCAS.

CLEAR AS PER IP-0006, 3.10 DO NOT DESELECT THE CRACKS.

	4
	REPAIR SHOP	TRATAMENTO TERMICO / HEAT TREATMENT	EXECUTAR TRATAMENTO TÉRMICO EM 1010 ° C POR 30 MINUTOS.

PERFORM HEAT TREATMENT AT 1010°C FOR 30 MINUTES.

	5
	REPAIR SHOP	SOLDAR / WELDING	           SOLDAR AS TRINCAS ASSINALADAS, COM AMS 5798

WELD THE MARKED CRACKS WITH AMS 5798

	6
	REPAIR SHOP	SOLDAR / WELDING	REMOVER O FUEL FERRULE DESGASTADO E SOLDAR (AMS 5798) O NOVO P/N=6855575

REMOVE THE WORN FUEL FERRULE AND WELD (AMS 5798) THE NEW P/N=6855575

	7
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	SUAVISAR AS SOLDAS.

SOFTENING THE SOLDIERS.

	8
	REPAIR SHOP	TRATAMENTO TERMICO / HEAT TREATMENT	EXECUTAR TRATAMENTO TÉRMICO EM 1010 ° C POR 30 MINUTOS.

PERFORM HEAT TREATMENT AT 1010°C FOR 30 MINUTES.

	9
	NDT	END- LIQUIDO PENETRANTE / NDT - FLUORESCENT PENETRANT INSPECTION	EXECUTAR FPI: ASTM E 1417, METHOD-A, LEVEL-3.
APRESENTOU INDICAÇÃO? (  )SIM     (  )NÃO

RUN FPI: ASTM E 1417, METHOD-A, LEVEL-3. DID YOU PRESENT AN INDICATION? ( )YES ( )NO

	10
	CHEMICAL CLEANING	LIMPAR / CLEAN	LIMPAR CONFORME A IP-0006, 3.10

CLEAR AS PER IP-0006, 3.10

	11
	T56A	INSPEÇÃO / INSPECTION	INSPEÇÃO FINAL.
(  )APROVADO         (  )REPROVADO

FINAL INSPECTION. ( )APPROVED ( )FAILED
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