| PN (PN): |  |  | SN: |  |  |  |  | Nº da OS (WO): |  |  | TLN:02188 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 6842873 |  |  | A-6062 |  |  |  |  | IAS |  |  |  |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  |  | ARTIGO/PARTE (Article/Part): |  |  | Serviço PrincipaL (Main Service) |  | QUANT: |  |  |
| IAS / AE-108636 |  |  |  | DIFFUSER |  |  | REVISÃO GERAL / OVERHAUL |  | 1 |  |  |
| ITEM (Item) | TAREFA (Task) | ETAPA (Step) |  |  | DESCRIÇÃO (Description) |  |  |  |  |  |  |
| 1 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 2 | NDT | END- LIQUIDO PENETRANTE / NDT - FLUORESCENT PENETRANT INSPECTION |  |  | EXECUTAR FPI: ASTM E 1417, METHOD-A, LEVEL 3. APRESENTOU INDICAÇÃO? ( )SIM ( )NÃO RUN FPI: ASTM E 1417, METHOD-A, LEVEL 3. DID YOU PRESENT AN INDICATION? ( )YES ( )NO |  |  |  |  |  |  |
| 3 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 4 | REPAIR SHOP | SOLDAR / WELDING |  |  | INSTALAR A BAFFLE INTERNA, PONTEANDO COM: AMS 5776, 5680, 5782 Ou 5784. INSTALL THE INTERNAL BAFFLE, POINTING TO: AMS 5776, 5680, 5782 OR 5784. |  |  |  |  |  |  |
| 5 | T56A | INSPEÇÃO / INSPECTION |  |  | INSPEÇÃO VISUAL E CONFERIR O LAUDO DE END. VISUAL INSPECTION AND CHECK THE END REPORT. |  |  |  |  |  |  |
| 6 | REPAIR SHOP | ISOLAÇÃO / MASK |  |  | ISOLAR AS ROSCAS, FUROS E ÁREAS DE CONTATO. ISOLATE THREADS, HOLES, AND CONTACT AREAS. |  |  |  |  |  |  |
| 7 | REPAIR SHOP | PINTURA / PAINTING |  |  | PINTAR EXTERNAMENTE COM SERMETEL W, CONFORME A IP-0006, 3.17 PAINTING EXTERNALLY WITH SERMETEL W IN ACCORDANCE WITH IP-0006, 3.17 |  |  |  |  |  |  |
| 8 | Escolher um item. | Escolher um item. |  |  | REMOVER AS ISOLAÇÕES E OS EXCESSOS DE SERMETE. REMOVE INSULATION AND EXCESS SERMETE. |  |  |  |  |  |  |
| 9 | REPAIR SHOP | REMOÇÃO / REMOVE |  |  | REMOVER A SLEEVE, LIMPAR AS ÁREAS DE CONTATO E REINSTALA-LA SEM FRENAR. REMOVE THE SLEEVE, CLEAN THE CONTACT AREAS AND REINSTALL IT WITHOUT BRAKING. |  |  |  |  |  |  |
| 10 | T56A | TESTE /TEST |  |  | TESTE DE PRESSÃO. PRESSURE TEST. |  |  |  |  |  |  |
| 11 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | FRENAR A SLEEVE COM 2- PINOS P/N= 6739977 BRAKING THE SLEEVE WITH 2- PINS P/N= 6739977 |  |  |  |  |  |  |
| 12 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | POLIR AS ROSCAS E AS ÁREAS DE CONTATO. POLISH THE THREADS AND CONTACT AREAS. |  |  |  |  |  |  |
| 13 | T56A | INSPEÇÃO / INSPECTION |  |  | INSPEÇÃO FINAL. USAR NO MOTOR 501D22A ( )APROVADO ( )REPROVADO FINAL INSPECTION. ( )APPROVED ( )FAILED |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  | DATA (Date): |  |
|  |  |  |  |  |  | VILSON BARBOSA |  |  |  | 16/09/2025 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)