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	PN (PN):
	SN:
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	Nº DO ARTIGO PRINCIPAL (Main Article):
	ARTIGO/PARTE (Article/Part):
	Serviço PrincipaL
(Main Service)
	QUANT:

	AE- 108636
	   COMPRESSOR WHEEL 14º ST
	REVISÃO GERAL / OVERHAUL	1

	
	
	
	

	ITEM
(Item)
	[bookmark: _Hlk184222911]TAREFA
(Task)
	[bookmark: _Hlk184222919]ETAPA
(Step)
	DESCRIÇÃO
(Description)

	1
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	REMOVER TODAS AS PALHETAS COM CUIDADO, POIS SERÃO REAPROVEITADAS.

REMOVER TODOS PEDAÇOS DE PINOS FRENOS E O CONTRA PESO, SUAVISANDO OS FUROS DO LIP.

REMOVE ALL THE REEDS CAREFULLY, AS THEY WILL BE REUSED. REMOVE ALL PIECES OF BRAKE PINS AND THE COUNTERWEIGHT, SMOOTHING THE LIP HOLES.

	2
	CHEMICAL CLEANING	LIMPAR / CLEAN	LIMPAR CONFORME A IP-0006, 3.10

CLEAR AS PER IP-0006, 3.10

	3
	NDT	END- LIQUIDO PENETRANTE / NDT - FLUORESCENT PENETRANT INSPECTION	EXECUTAR FPI: ASTM E 1417, METHOD-D, LEVEL-4.
APRESENTOU INDICAÇÃO?  (  )SIM     (  )NÃO

RUN FPI: ASTM E 1417, METHOD-D, LEVEL-4. DID YOU PRESENT AN INDICATION? ( )YES ( )NO

	4
	CHEMICAL CLEANING	LIMPAR / CLEAN	LIMPAR CONFORME A IP-0006, 3.10

CLEAR AS PER IP-0006, 3.10

	5
	NDT	END- PARTICULAS MAGNETICAS / NOT - MAGNETIC PARTICLE	EXECUTAR MPI: ASTM E 1444.
APRESENTOU INDICAÇÃO?   (  )SIM    (  )NÃO

RUN MPI: ASTM E 1444. DID YOU PRESENT AN INDICATION? ( )YES ( )NO

	6
	CHEMICAL CLEANING	LIMPAR / CLEAN	                              LIMPAR CONFORME A IP-0006, 3.10

CLEAR AS PER IP-0006, 3.10

	7
	CHEMICAL CLEANING	DEPOSIÇÃO DE PRATA/ SILVER PLATING	
ISOLAR O EIXO E A RODA E APLICAR BANHO DE PRATA (IT-0279) NA ROSCA INTERNA, CONFORME MOSTRA A FIGURA DA PÁGINA 925 ANEXA.

ISOLATE THE AXLE AND WHEEL AND APPLY SILVER PLATING (IT-0279) TO THE INTERNAL THREAD, AS SHOWN IN THE FIGURE ON PAGE 925 ENCLOSED.

	8
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	INSTALAR AS PALHETAS E FRENA-LAS COM OS PINOS P/N=6731108
 EXECUTANDO STAC NO FINAL.

INSTALL THE BLADES AND BRAKE THEM WITH THE P/N=6731108 RUNNING STAC AT THE END.

	9
	T56A	INSPEÇÃO / INSPECTION	                             INSPEÇÃO FINAL.
(  )APROVADO       (  )REPROVADO

FINAL INSPECTION. ( )APPROVED ( )FAILED

	OBSERVAÇÕES
(Observation):
	ASSINATURA DO SOLICITANTE 
(Signature):
	DATA 23/09/2025
(Date):

	[bookmark: Texto2]     
	VILSON BARBOSA
	23/09/2025


· Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.
(In case of external service, the supplier must be indicated by the purchasing department)
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