| PN (PN): |  |  | SN: |  |  |  |  | Nº da OS (WO): |  |  | TLN:02188 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 6841214 |  |  | RR6527A |  |  |  |  | IAS |  |  |  |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  |  | ARTIGO/PARTE (Article/Part): |  |  | Serviço PrincipaL (Main Service) |  | QUANT: |  |  |
| AE- 109020 |  |  |  | COMPRESSOR WHEEL 4º ST |  |  | REVISÃO GERAL / OVERHAUL |  | 1 |  |  |
| ITEM (Item) | TAREFA (Task) | ETAPA (Step) |  |  | DESCRIÇÃO (Description) |  |  |  |  |  |  |
| 1 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | REMOVER 5- PALHETAS REFUGOS VERMELHAS. REMOVER AS DEMAIS PALHETAS BOAS COM CUIDADO, POIS SERÃO REAPROVEITADAS. REMOVER TODOS PEDAÇOS DE PINOS FRENOS. REMOVE 5- RED WASTE STRAWS. REMOVE THE OTHER GOOD STRAWS CAREFULLY, AS THEY WILL BE REUSED. REMOVE ALL PIECES OF FRENOS PINS. |  |  |  |  |  |  |
| 2 | CHEMICAL CLEANING | JATEAR / BLAST |  |  | APLICAR GLASS BEAD GERAL, CONFORME A IP-0006, 3.26 APPLY GLASS BEAD GENERAL, ACCORDING TO IP-0006, 3.26 |  |  |  |  |  |  |
| 3 | NDT | END- LIQUIDO PENETRANTE / NDT - FLUORESCENT PENETRANT INSPECTION |  |  | EXECUTAR FPI: ASTM E 1417, METHOD-D, LEVEL-4. APRESENTOU INDICAÇÃO? ( )SIM ( )NÃO RUN FPI: ASTM E 1417, METHOD-D, LEVEL-4. DID YOU PRESENT AN INDICATION? ( )YES ( )NO |  |  |  |  |  |  |
| 4 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 5 | NDT | END- PARTICULAS MAGNETICAS / NOT - MAGNETIC PARTICLE |  |  | EXECUTAR MPI: ASTM E 1444. APRESENTOU INDICAÇÃO? ( )SIM ( )NÃO RUN MPI: ASTM E 1444. DID YOU PRESENT AN INDICATION? ( )YES ( )NO |  |  |  |  |  |  |
| 6 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 7 | CHEMICAL CLEANING | DEPOSIÇÃO DE NIQUEL-CADMIO / NICKEL-CADMIUM PLATING |  |  | APLICAR BANHO DE NICKEL CÁDMIO, AMS 2416. APPLY NICKEL CADMIUM BATH, AMS 2416. |  |  |  |  |  |  |
| 8 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | INSTALAR AS PALHETAS E NÃO FRENAR. INSTALL THE BLADES AND DO NOT BRAKE. |  |  |  |  |  |  |
| 9 | REPAIR SHOP | BALANCEAMENTO / BALANCING |  |  | CONFERIR E INFORMAR O PONTO E O VALOR DO DESBALANCEAMENTO. CHECK AND INFORM THE POINT AND VALUE OF THE UNBALANCE. |  |  |  |  |  |  |
| 10 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | FRENAR AS PALHETAS COM OS PINOS P/N=6783397 E EXECUTAR STAC. BRAKE THE BLADES WITH THE P/N=6783397 AND RUN STAC. |  |  |  |  |  |  |
| 11 | T56A | INSPEÇÃO / INSPECTION |  |  | INSPEÇÃO FINAL. ( )APROVADO ( )REPROVADO FINAL INSPECTION. ( )APPROVED ( )FAILED |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  | DATA 25/09/2025 (Date): |  |
|  |  |  |  |  |  | VILSON BARBOSA |  |  |  | 25/09/2025 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)