| PN (PN): |  |  | SN: |  |  |  |  | Nº da OS (WO): |  |  | TLN:02188 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 6792769 |  |  | RR6368 |  |  |  |  | IAS |  |  |  |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  |  | ARTIGO/PARTE (Article/Part): |  |  | Serviço PrincipaL (Main Service) |  | QUANT: |  |  |
| AE- 109696 |  |  |  | COMPRESSOR WHEEL 9° ST. |  |  | REVISÃO GERAL / OVERHAUL |  | 1 |  |  |
| ITEM (Item) | TAREFA (Task) | ETAPA (Step) |  |  | DESCRIÇÃO (Description) |  |  |  |  |  |  |
| 1 | CHEMICAL CLEANING | DECAPAGEM / STRIPPING |  |  | REMOVER O BANHO DE NICKEL CÁDMIO. REMOVE THE NICKEL CADMIUM BATH. |  |  |  |  |  |  |
| 2 | NDT | END- LIQUIDO PENETRANTE / NDT - FLUORESCENT PENETRANT INSPECTION |  |  | EXECUTAR FPI: ASTM E 1417, METHOD-D, LEVEL-4. APRESENTOU RUN FPI: ASTM E 1417, METHOD-D, LEVEL-4. PRESENTED |  |  |  |  |  |  |
| 3 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 4 | NDT | END- PARTICULAS MAGNETICAS / NOT - MAGNETIC PARTICLE |  |  | EXECUTAR MPI: ASTM E 1444. APRESENTOU INDICAÇÃO? ( )SIM ( )NÃO RUN MPI: ASTM E 1444. DID YOU PRESENT AN INDICATION? ( )YES ( )NO |  |  |  |  |  |  |
| 5 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 6 | CHEMICAL CLEANING | DEPOSIÇÃO DE NIQUEL-CADMIO / NICKEL-CADMIUM PLATING |  |  | APLICAR BANHO DE NICKEL CÁDMIO, AMS 2416. APPLY NICKEL CADMIUM BATH, AMS 2416. |  |  |  |  |  |  |
| 7 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | INSTALAR AS PALHETAS, MAS NÃO FRENA-LAS. INSTALL THE VANES, BUT DO NOT BRAKE THEM. |  |  |  |  |  |  |
| 8 | REPAIR SHOP | BALANCEAMENTO / BALANCING |  |  | CONFERIR E INFORMAR O PONTO E O VALOR DO DESBALANCEAMENTO. CHECK AND INFORM THE POINT AND VALUE OF THE UNBALANCE. |  |  |  |  |  |  |
| 9 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | FRENAR AS PALHETAS COM OS PINOS P/N= 6730907 E EXECUTAR STAK. BRAKE THE VANES WITH THE PINS P/N= 6730907 AND PERFORM STAK. |  |  |  |  |  |  |
| 10 | T56A | INSPEÇÃO / INSPECTION |  |  | INSPEÇÃO FINAL. ( )APROVADO ( )REPROVADO FINAL INSPECTION. ( )APPROVED ( )FAILED |  |  |  |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  | DATA 01/10/2025 (Date): |  |
|  |  |  |  |  |  | VILSON BARBOSA |  |  |  | 01/10/2025 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)