| PN (PN): |  |  | SN: |  |  |  |  | Nº da OS (WO): |  |  | TLN:02188 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 23035961 |  |  | 24182 |  |  |  |  | IAS |  |  |  |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  |  | ARTIGO/PARTE (Article/Part): |  |  | Serviço PrincipaL (Main Service) |  | QUANT: |  |  |
| AE- 108636 |  |  |  | REAR BEARING SUPPORT |  |  | REVISÃO GERAL / OVERHAUL |  | 1 |  |  |
| ITEM (Item) | TAREFA (Task) | ETAPA (Step) |  |  | DESCRIÇÃO (Description) |  |  |  |  |  |  |
| 1 | REPAIR SHOP | SOLDAR / WELDING |  |  | SOLDAR AS TRINCAS, QUE AS FOTOS DO ¨FPI¨ MOSTRAM. AMS 5786 ou AMS 5674 (347SS) SUAVISAR AS SOLDAS, CANTOS VIVOS. WELD THE CRACKS, WHICH THE PHOTOS OF THE ̈FPI ̈ SHOW. AMS 5786 or AMS 5674 (347SS) SMOOTH WELDS, SHARP CORNERS. |  |  |  |  |  |  |
| 2 | REPAIR SHOP | SOLDAR / WELDING |  |  | REFORÇAR COM SOLDA OS 4- KEY SLOTS. AMS 5786 ou AMS 5674 (347SS) REINFORCE WITH SOLDERING THE 4-KEY SLOTS. AMS 5786 or AMS 5674 (347SS) |  |  |  |  |  |  |
| 3 | REPAIR SHOP | TRATAMENTO TERMICO / HEAT TREATMENT |  |  | TRATAMENTO TÉRMICO EM 650°C POR 3- HORAS. HEAT TREATMENT AT 650°C FOR 3-HOURS. |  |  |  |  |  |  |
| 4 | NDT | END- LIQUIDO PENETRANTE / NDT - FLUORESCENT PENETRANT INSPECTION |  |  | EXECUTAR FPI: ASTM E 1417, METHOD-A, LEVEL-3. RUN FPI: ASTM E 1417, METHOD-A, LEVEL-3. |  |  |  |  |  |  |
| 5 | REPAIR SHOP | JATEAR / BLAST |  |  | SHOT PEEN NAS SOLDAS (SIZE 0.020¨) INTENSITY= 10A, AMS 2430. SHOT PEEN NAS SOLDAS (SIZE 0.020¨) INTENSITY= 10A, AMS 2430. |  |  |  |  |  |  |
| 6 | REPAIR SHOP | USINAGEM / MACHINING |  |  | USINAR AS SOLDAS NOS 4-KEY SLOTS (RASGO: LARGURA=0.240¨, PROFUNDIDADE=0.120¨ e FURO=0.220¨) VEJA A FIGURA ANEXA. USINAR AS SOLDAS NOS 4-KEY SLOTS (TRAIT: LENGTH=0.240 ̈, DEPTH=0.120 ̈ and FURY=0.220 ̈) SEE THE ATTACHED FIGURE. |  |  |  |  |  |  |
| 7 | REPAIR SHOP | USINAGEM / MACHINING |  |  | USINAR A FACE- L, M e o DIÂMETRO- J, DEIXANDO 2/3 DE MANCHAS. REMOVER O CANTO VIVO. MACHINE THE FACE- L, M and the DIAMETER- J, LEAVING 2/3 OF STAINS. REMOVE THE LIVE CORNER. |  |  |  |  |  |  |
| 8 | T56A | INSPEÇÃO / INSPECTION |  |  | INSPEÇÃO FINAL. ( )APROVADO ( )REPROVADO FINAL INSPECTION. ( )APPROVED ( )FAILED |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  | DATA 13/10/2025 (Date): |  |
|  |  |  |  |  |  | VILSON BARBOSA |  |  |  | 13/10/2025 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)