| PN (PN): |  |  | SN: |  |  |  |  | Nº da OS (WO): |  |  | TLN:02188 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 23001195 |  |  | XX13314 |  |  |  |  | IAS |  |  |  |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  |  | ARTIGO/PARTE (Article/Part): |  |  | Serviço PrincipaL (Main Service) |  | QUANT: |  |  |
| AE- 108636 |  |  |  | REAR CASE |  |  | REVISÃO GERAL / OVERHAUL |  | 1 |  |  |
| ITEM (Item) | TAREFA (Task) | ETAPA (Step) |  |  | DESCRIÇÃO (Description) |  |  |  |  |  |  |
| 1 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 2 | NDT | END- LIQUIDO PENETRANTE / NDT - FLUORESCENT PENETRANT INSPECTION |  |  | EXECUTAR FPI: ASTM E 1417, METHOD-A, LEVEL-3. PRESTAR ESPECIAL ATENÇÃO NAS ÁREAS DE ESTRESSES, CONFORME MOSTRA A FIGURA ANEXA. APRESENTOU INDICAÇÃO? ( )SIM ( )NÃO RUN FPI: ASTM E 1417, METHOD-A, LEVEL-3. PAY SPECIAL ATTENTION TO AREAS OF STRESS, AS SHOWN IN THE ATTACHED FIGURE. DID YOU PRESENT AN INDICATION? ( )YES ( )NO |  |  |  |  |  |  |
| 3 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | LIMPAR CONFORME A IP-0006, 3.10 CLEAR AS PER IP-0006, 3.10 |  |  |  |  |  |  |
| 4 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | PASSAR ALARGADOR NOS 2- FUROS ONDE PASSAM OS EYE BOLTS. VEJA A FIGURA ANEXA. PASSAR UMA BROCA DE 0.312¨ NOS FUROS DA FACE MAIOR, ADJACENTES AOS STUDS DE UNIÃO. APPLY REAMER IN THE 2- HOLES WHERE THE EYE BOLTS PASS. SEE THE ATTACHED FIGURE. PASS A 0.312 ° DRILL BIT INTO THE HOLES ON THE LARGER FACE, ADJACENT TO THE JOINING STUDS. |  |  |  |  |  |  |
| 5 | REPAIR SHOP | ISOLAÇÃO / MASK |  |  | ISOLAR OS STUDS, INSERTS, FUROS E ÁREAS DE CONTATO. ISOLATE STUDS, INSERTS, HOLES AND CONTACT AREAS. |  |  |  |  |  |  |
| 6 | REPAIR SHOP | PINTURA / PAINTING |  |  | PINTAR EXTERNAMENTE: PRIMER PA-0060 CINZA PA-0065 PAINTING EXTERNALLY: FIRST PA-0060 CINZA PA-0065 |  |  |  |  |  |  |
| 7 | REPAIR SHOP | REMOVER ISOLAMENTO / REMOVE MASK |  |  | REMOVER AS ISOLAÇÕES E OS EXCESSOS DE TINTA. REMOVE INSULATION AND EXCESS PAINT. |  |  |  |  |  |  |
| 8 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | LIMPAR AS ROSCAS DOS STUDS E INSERTS. CLEAN THE THREADS OF THE STUDS AND INSERTS. |  |  |  |  |  |  |
| 9 | CHEMICAL CLEANING | INSPEÇÃO / INSPECTION |  |  | LIMPAR COM PRESSÃO TODAS AS ENTRANÇAS E VIAS. IP-0006, 3.9 PRESSURE CLEAN ALL BRAIDS AND TRACKS. IP-0006, 3.9 |  |  |  |  |  |  |
| 10 | T56A | INSPEÇÃO / INSPECTION |  |  | INSPEÇÃO FINAL. ( )APROVADO ( )REPROVADO FINAL INSPECTION. ( )APPROVED ( )FAILED |  |  |  |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  | DATA 15/10/2025 (Date): |  |
|  |  |  |  |  |  | VILSON BARBOSA |  |  |  | 15/10/2025 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)