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	Nº DO ARTIGO PRINCIPAL (Main Article):
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	AE- 108598
	                HOUSING COUPLING
	REVISÃO GERAL / OVERHAUL	1

	
	
	
	

	ITEM
(Item)
	[bookmark: _Hlk184222911]TAREFA
(Task)
	[bookmark: _Hlk184222919]ETAPA
(Step)
	DESCRIÇÃO
(Description)

	1
	REPAIR SHOP	REPAROS MANUAIS / MANUAL REPAIR	REMOVER COM LIXA AS REBARBAS DO BOCAL E 
APAGAR COM LIXA AS ESCRITAS EXTERNAS, DEIXANDO APENAS O P/N=6823502 e o S/N=A11164.

REMOVE BURRS FROM THE NOZZLE WITH SANDPAPER AND ERASE THE EXTERNAL WRITINGS WITH SANDPAPER, LEAVING ONLY THE P/N=6823502 and the S/N=A11164.

	2
	NDT	END- PARTICULAS MAGNETICAS / NOT - MAGNETIC PARTICLE	EXECUATR MPI: ASTM E 1444.
APRESENTOU INDICAÇÃO?   (  )SIM      (  )NÃO

EXECUATR MPI: ASTM E 1444. DID YOU PRESENT AN INDICATION? ( )YES ( )NO

	3
	CHEMICAL CLEANING	LIMPAR / CLEAN	LIMPAR CONFORME A IP-0006, 3.10

CLEAR AS PER IP-0006, 3.10

	4
	NDT	END- LIQUIDO PENETRANTE / NDT - FLUORESCENT PENETRANT INSPECTION	EXECUTAR FPI: ASTM E 1417, METHOD-A, LEVEL-3.
APRESENTOU INDICAÇÃO?  (  )SIM    (  )NÃO

RUN FPI: ASTM E 1417, METHOD-A, LEVEL-3. DID YOU PRESENT AN INDICATION? ( )YES ( )NO

	5
	CHEMICAL CLEANING	LIMPAR / CLEAN	LIMPAR CONFORME A IP-0006, 3.10

CLEAR AS PER IP-0006, 3.10

	6
	REPAIR SHOP	RETIFICA / RECTIFY	RETIFICAR O DIÂMETRO INTERNO ¨A¨, DEIXANDO COM 2.511¨ +ou- 0.002¨
CENTRAR PELO ¨B¨, VEJA A FIGURA ANEXA.

RECTIFY THE INTERNAL DIAMETER ̈A ̈, LEAVING 2.511 ̈ + OR- 0.002 ̈ CENTER BY THE "B", SEE THE ATTACHED FIGURE.

	7
	CHEMICAL CLEANING	DEPOSIÇÃO DE CROMO / CHROME PLATING	APLICAR CROMO DURO NO DIÂMETRO INTERNO ¨A¨, (2.500¨)

APPLY HARD CHROME TO THE INNER DIAMETER ̈A ̈, (2,500 ̈)

	8
	CHEMICAL CLEANING	TRATAMENTO TERMICO / HEAT TREATMENT	TRATAMENTO TÉRMICO EM 190°C POR 3- HORAS.

HEAT TREATMENT AT 190°C FOR 3- HOURS.

	9
	REPAIR SHOP	RETIFICA / RECTIFY	RETIFICAR O DIÂMETRO INTERNO ¨A¨CROMADO, DEIXANDO CENTRADO PELO ¨B¨ e com 2.5005¨+ou- 0.0005¨
REMOVER OS CANTOS VIVOS.  VEJA A FIGURA ANEXA.

RECTIFY THE INTERNAL DIAMETER ̈A ̈CHROME, LEAVING IT CENTERED BY THE ̈B ̈ and with 2.5005 ̈+or- 0.0005 ̈ REMOVE SHARP CORNERS. SEE THE ATTACHED FIGURE.

	10
	CHEMICAL CLEANING	JATEAR / BLAST	APLICAR GLASS BEAD EXTERNAMENTE, CONFORME A IP-0006, 3.26

APPLY GLASS BEAD EXTERNALLY, CONFORMING TO IP-0006, 3.26
APPLY GLASS BEAD EXTERNALLY, CONFORMING TO IP-0006, 3.26

	11
	CHEMICAL CLEANING	DEPOSIÇÃO DE ANODIZAÇÃO / ANODIZING PLATING	APLICAR OXIDAÇÃO NEGRA.

APPLY BLACK OXIDATION.

	12
	T56A	INSPEÇÃO / INSPECTION	INSPEÇÃO FINAL.
(  )APROVADO    (  )REPROVADO

FINAL INSPECTION. ( )APPROVED ( )FAILED

	OBSERVAÇÕES
(Observation):
	ASSINATURA DO SOLICITANTE 
(Signature):
	DATA 17/10/2025
(Date):

	[bookmark: Texto2]     
	VILSON BARBOSA
	17/10/2025


· Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.
(In case of external service, the supplier must be indicated by the purchasing department)
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