| PN (PN): |  |  | SN: |  |  |  |  | Nº da OS (WO): |  |  | TLN:02188 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 6873624 |  |  | B415 |  |  |  |  | IAS |  |  |  |
| Nº DO ARTIGO PRINCIPAL (Main Article): |  |  |  | ARTIGO/PARTE (Article/Part): |  |  | Serviço PrincipaL (Main Service) |  | QUANT: |  |  |
| AE- 109020 |  |  |  | INLET VANE |  |  | REVISÃO GERAL / OVERHAUL |  | 1 |  |  |
| ITEM (Item) | TAREFA (Task) | ETAPA (Step) |  |  | DESCRIÇÃO (Description) |  |  |  |  |  |  |
| 1 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | EXECUTAR LIMPEZA, CONFORME A IP-0006, 3.10 PERFORM CLEANING, ACCORDING TO IP-0006, 3.10 |  |  |  |  |  |  |
| 2 | NDT | END- LIQUIDO PENETRANTE / NDT - FLUORESCENT PENETRANT INSPECTION |  |  | EXECUTAR FPI: ASTM E 1417, METHOD-A, LEVEL-3. APRESENTOU INDICAÇÃO? ( )SIM ( )NÃO RUN FPI: ASTM E 1417, METHOD-A, LEVEL-3. DID YOU PRESENT AN INDICATION? ( )YES ( )NO |  |  |  |  |  |  |
| 3 | CHEMICAL CLEANING | LIMPAR / CLEAN |  |  | EXECUTAR LIMPEZA, CONFORME A IP-0006, 3.10 PERFORM CLEANING, ACCORDING TO IP-0006, 3.10 |  |  |  |  |  |  |
| 4 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | RASPAR A RESINA QUE ESTIVER SOLTANDO NAS UNIÃOS DAS ALHETAS COM OS RINGS E APLICAR NOVO ADESIVO, SCOTCH-WELD STRUCTURAL 2214 HI TEMP (CAGE 04963) SCRAPE OFF THE RESIN THAT IS LOOSENING AT THE JUNCTIONS OF THE FINS WITH THE RINGS AND APPLY NEW ADHESIVE, SCOTCH-WELD STRUCTURAL 2214 HI TEMP (CAGE 04963) |  |  |  |  |  |  |
| 5 | REPAIR SHOP | REPAROS MANUAIS / MANUAL REPAIR |  |  | POLIR COM LIXA FINA O BORDO DE ATAQUE DAS ALHETAS. POLISH THE LEADING EDGE OF THE FINS WITH FINE SANDPAPER. |  |  |  |  |  |  |
| 6 | REPAIR SHOP | SOLDAR / WELDING |  |  | AMASSAR AS PONTAS ASSINALADAS DE AZUL PARA REDUZIR A ENTRADA DE AR EXTERNAMENTE E APLICAR UM FINO CORDÃO DE SOLDA (AMS 5784) PARA FECHAR E SUAVISAR A SOLDA. KNEAD THE TIPS MARKED BLUE TO REDUCE THE ENTRY OF AIR EXTERNALLY AND APPLY A THIN WELD BEAD (AMS 5784) TO CLOSE AND SMOOTH THE WELD. |  |  |  |  |  |  |
| 7 | REPAIR SHOP | USINAGEM / MACHINING |  |  | USINAR O DIÂMETRO INTERNO DO OUTER RING, ATÉ UMA DISTÂNCIA DE 4 mm DAS ALHETAS, DEIXANDO 80% DE MANCHA. REMOVER CANTO VIVO. MACHINE THE INNER DIAMETER OF THE OUTER RING, DOWN TO A 4 MM DISTANCE FROM THE FINS, LEAVING 80% STAIN. REMOVE LIVE CORNER. |  |  |  |  |  |  |
| 8 | T56A | INSPEÇÃO / INSPECTION |  |  | INSPEÇÃO FINAL. ( )APROVADO ( )REPROVADO FINAL INSPECTION. ( )APPROVED ( )FAILED |  |  |  |  |  |  |
|  | Escolher um item. | Escolher um item. |  |  |  |  |  |  |  |  |  |
| OBSERVAÇÕES (Observation): |  |  |  |  |  | ASSINATURA DO SOLICITANTE (Signature): |  |  |  | DATA 21/10/2025 (Date): |  |
|  |  |  |  |  |  | VILSON BARBOSA |  |  |  | 21/10/2025 |  |

- Em caso de serviço externo, o fornecedor deverá ser indicado pelo setor de compras.

(In case of external service, the supplier must be indicated by the purchasing department)